10

speciic load [N/mm²]

1

0.1

0.01

0.001

Diepolast dyn series

## Working range

S 75

S 150

S 350

S 750

S 1500

Diepolast dyn type

## Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.075

Dynamic load: up to [N/mm²]

0.120

Load peaks: up to [N/mm²]

2.0

Values depending on form factor and apply to form factor q = 3

## Material	closed cellular polyether-urethane

Colour	yellow

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m long

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.06 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 0.63 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 0.92 N/mm² | DIN 53513 (2) |  |
| Static shear modulus (1) | 0.16 N/mm² | DIN 53513 (2) | preload 0.075 N/mm² |
| Dynamic shear modulus (1) | 0.27 N/mm² | DIN 53513 (2) | preload 0.075 N/mm², 10 Hz |
| Resistance to strain | 0.083 N/mm² |  | at 10% deformation |
| Residual compression set | < 5 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 1.5 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 500 % | DIN 53455-6-4 | minimum |
| Tear resistance | > 1.6 N/mm | DIN ISO 34-1/A |  |
| Rebound elasticity | 70 % | DIN EN ISO 8307 | ± 10% |
| Speciic volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.06 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 up to +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inlammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal lammable |

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

## Load deflection curve

0.15

Specific load [N/mm²]

0.10

0.05

0.00

0	2	4	6	8	10	12

### Recording of the 3rd loading; testing between steel plates at room temperature measured with a delection rate of 1% of the thickness per second

Form factor q = 3

Deflection [mm]

## Modulus of elasticity

1.4

1.2

Mo d u l u s of elasticity [N/mm²]

1.0

0.8

0.6

0.4

0.2

0.0

0.00	0.05	0.10	0.15

### Dynamic test: sinusoidal excitation with an oscilla- ting range of ± 0.11 mm at 10 Hz and ± 0.04 mm at 30 Hz

Quasistatic modulus of elasticity:

tangent modulus taken from the load delection curve

Test according to DIN 53513 Form factor q = 3

Specific load [N/mm²]

## Natural frequency

0.15

Specific load [N/mm²]

0.10

0.05

0.00

0	5	10	15	20	25

### Natural frequency of a single-degree-of-freedom system consisting of a ixed mass and an elastic bearing consisting of Diepolast dyn S 75 on

a stiff subgrade. Form factor q = 3

Natural frequency [Hz]

## Correction values varying form factors

### s p eciic load 0.075 N/mm², form factor q = 3

Static load range	Deflection

0.080

Specific load [N/mm²]

0.075

0.070

0.065

0.060

0.3	1	3	10

F orm factor

### Dynamic modulus of elasticity at 10 Hz	Natural frequency

DISCLAIMER:

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast dyn products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certiied testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

10

speciic load [N/mm²]

1

0.1

0.01

0.001

Diepolast dyn series

## Working range

S 75

S 150

S 350

S 750

S 1500

Diepolast dyn type

## Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.150

Dynamic load: up to [N/mm²]

0.250

Load peaks: up to [N/mm²]

3.0

Values depending on form factor and apply to form factor q = 3

## Material	closed cellular polyether-urethane

Colour	green

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m long

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.03 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 1.25 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 1.65 N/mm² | DIN 53513 (2) |  |
| Static shear modulus (1) | 0.22 N/mm² | DIN 53513 (2) | preload 0.15 N/mm² |
| Dynamic shear modulus (1) | 0.35 N/mm² | DIN 53513 (2) | preload 0.15 N/mm², 10 Hz |
| Resistance to strain | 0.16 N/mm² |  | at 10% deformation |
| Residual compression set | < 5 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 2.0 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 500 % | DIN 53455-6-4 | minimum |
| Tear resistance | > 2.1 N/mm | DIN ISO 34-1/A |  |
| Rebound elasticity | 70 % | DIN EN ISO 8307 | ± 10% |
| Speciic volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.075 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 up to +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inlammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal lammable |

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

## Load deflection curve

0.30

0.25

Specific load [N/mm²]

0.20

0.15

0.10

0.05

0.00

0	2	4	6	8	10	12

### Recording of the 3rd loading; testing between steel plates at room temperature measured with a delection rate of 1% of the thickness per second

Form factor q = 3

Deflection [mm]

## Modulus of elasticity

3.0

M o d u l u s of elasticity [N/mm²]

2.5

2.0

1.5

1.0

0.5

0.0

0.00	0.05	0.10	0.15	0.20	0.25	0.30

### Dynamic test: sinusoidal excitation with an oscilla- ting range of ± 0.11 mm at 10 Hz and ± 0.04 mm at 30 Hz

Quasistatic modulus of elasticity:

tangent modulus taken from the load delection curve

Test according to DIN 53513 Form factor q = 3

Specific load [N/mm²]

## Natural frequency

0.30

0.25

S p e c ific load [N/mm²]

0.20

0.15

0.10

0.05

0.00

50 mm

37.5 mm

25 mm

12.5 mm

0	5	10	15	20	25

### Natural frequency of a single-degree-of-freedom system consisting of a ixed mass and an elastic bearing consisting of Diepolast dyn S 150 on

a stiff subgrade. Form factor q = 3

Natural frequency [Hz]

## Correction values varying form factors

### speciic load 0.15 N/mm², form factor q = 3

Static load range	Deflection

0.17

0.16

Specific load [N/mm²]

0.15

0.14

0.13

0.12

50

40

V ariation of deflection [ %

30

20

10

0

- 10

0.11

0.3	1	3

- 20

10

0. 3	1	3	10

For m f  actor	F orm factor

### Dynamic modulus of elasticity at 10 Hz	Natural frequency

n of the dynamic modulus of elasticity [%]

10

5

0

- 5

- 10

- 15

- 20

V ariatio

- 25

5

Variation of th e natural frequency [%]

0

- 5

- 10

- 30

0.3	1	3

- 15

10

0.3	1	3	10

F or m factor	F orm factor

DISCLAIMER:

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast dyn products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certiied testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

10

speciic load [N/mm²]

1

0.1

0.01

0.001

Diepolast dyn series

S 150

S 750

Working range

S

350

S 75

Diepolast dyn type

## Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.350

Dynamic load: up to [N/mm²]

0.500

Load peaks: up to [N/mm²]

4.0

Values depending on form factor and apply to form factor q = 3

## Material	closed cellular polyether-urethane

S

1500

Colour	blue

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m long

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.03 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 2.53 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 3.25 N/mm² | DIN 53513 (2) |  |
| Static shear modulus (1) | 0,35 N/mm² | DIN 53513 (2) | preload 0.35 N/mm² |
| Dynamic shear modulus (1) | 0,52 N/mm² | DIN 53513 (2) | preload 0.35 N/mm², 10 Hz |
| Resistance to strain | 0.32 N/mm² |  | at 10% deformation |
| Residual compression set | < 5 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 3.5 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 500 % | DIN 53455-6-4 | minimum |
| Tear resistance | > 2.5 N/mm | DIN ISO 34-1/A |  |
| Rebound elasticity | 70 % | DIN EN ISO 8307 | ± 10% |
| Speciic volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.09 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 up to +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inlammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal lammable |

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

## Load deflection curve

0.8

Specific load [N/mm²]

0.6

0.4

0.2

0.0

0	2	4	6	8	10	12

### Recording of the 3rd loading; testing between steel plates at room temperature measured with a delection rate of 1% of the thickness per second

Form factor q = 3

Deflection [mm]

## Modulus of elasticity

6

Mo d u l u s of elasticity [N/mm²]

4

2

0

0. 0	0.2	0.4	0.6	0.8

### Dynamic test: sinusoidal excitation with an oscilla- ting range of ± 0.11 mm at 10 Hz and ± 0.04 mm at 30 Hz

Quasistatic modulus of elasticity:

tangent modulus taken from the load delection curve

Test according to DIN 53513 Form factor q = 3

Spe c i f i c  load [N/mm²]

## Natural frequency

0.8

Specific load [N/mm²]

0.6

0.4

0.2

0.0

0	5	10	15	20	25

### Natural frequency of a single-degree-of-freedom system consisting of a ixed mass and an elastic bearing consisting of Diepolast dyn S 350 on

a stiff subgrade. Form factor q = 3

Natural frequency [Hz]

## Correction values varying form factors

### speciic load 0.35 N/mm², form factor q = 3

Static load range	Deflection

0.38

0.36

Specific load [N/mm²]

0.34

0.32

0.30

0.28

50

40

Variation of deflection [ %

30

20

10

0

-10

0.26

0.3

1	3

For m facto

-20

10

0.3

1	3	10

Form factor

### Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

10

5

0

-5

-10

- 15

- 20

- 25

-    3 0

5

Variation of the n a t ural frequency [%]

0

-5

-10

-15

- 35

0.3	1	3

-20

10

0.3	1	3	10

Form factor	Fo r m factor

DISCLAIMER:

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast dyn products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certiied testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

10

speciic load [N/mm²]

1

0.1

0.01

0.001

Diepolast dyn series

## Working range

S

75

S

150

S

350

S

750

S

1500

Diepolast dyn type

## Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.750

Dynamic load: up to [N/mm²]

1.200

Load peaks: up to [N/mm²]

6.0

Values depending on form factor and apply to form factor q = 3

## Material	closed cellular polyether-urethane

Colour	red

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m long

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.04 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 5.21 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 8.88 N/mm² | DIN 53513 (2) |  |
| Static shear modulus (1) | 0.80 N/mm² | DIN 53513 (2) | preload 0.75 N/mm² |
| Dynamic shear modulus (1) | 1.22 N/mm² | DIN 53513 (2) | preload 0.75 N/mm², 10 Hz |
| Resistance to strain | 0.59 N/mm² |  | at 10% deformation |
| Residual compression set | < 6 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 5.0 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 500 % | DIN 53455-6-4 | minimum |
| Tear resistance | > 4.3 N/mm | DIN ISO 34-1/A |  |
| Rebound elasticity | 70 % | DIN EN ISO 8307 | ± 10% |
| Speciic volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.10 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 up to +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inlammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal lammable |

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

## Load deflection curve

1.6

Speciic load [N/mm2]

1.2

0.8

0.4

0.0

### Recording of the 3rd loading; testing between steel plates at room temperature measured with a delection rate of 1% of the thickness per second

Form factor q = 3

0	2	4	6	8	10	12

Delection [mm]

## Modulus of elasticity

15

Modulus of elasticity [N/mm2]

10

5

0

0.0	0.4	0.8	1.2	1.6

### Dynamic test: sinusoidal excitation with an oscilla- ting range of ± 0.11 mm at 10 Hz and ± 0.04 mm at 30 Hz

Quasistatic modulus of elasticity:

tangent modulus taken from the load delection curve

Test according to DIN 53513 Form factor q = 3

Speciic load [N/mm²]

## Natural frequency

1.6

Speciic load [N/mm2]

1.2

0.8

0.4

0.0

0	5	10	15	20	25

### Natural frequency of a single-degree-of-freedom system consisting of a ixed mass and an elastic bearing consisting of Diepolast dyn S 750 on

a stiff subgrade. Form factor q = 3

Natural frequency [Hz]

750

Diepolast dyn	S

# Prod	t	ata	eet

## Correction values varying form factors

### peciic load 0.75 N/mm², form factor q = 3

Static load range	Deflection

Dynamic modulus of elasticity at 10 Hz	Natural frequency

DISCLAIMER:

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast dyn products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certiied testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

P+S   oly   ethan-Ela tomere	Kielwe

Gmb	o KG	49356	ephol

Telefo	4   0	44	980-0	E-Mail: nfo@p	-poly rethan de

Telefa	4   0	44	980-80	Internet:   w w p	-poly ethan de

10

speciic load [N/mm²]

1

0.1

0.01

0.001

Diepolast dyn series

S 150

S 750

Working range

S

350

S 75

Diepolast dyn type

## Recommendations for elastic bearing:

Static load: up to [N/mm²]

1.500

Dynamic load: up to [N/mm²]

2.000

Load peaks: up to [N/mm²]

8.0

Values depending on form factor and apply to form factor q = 3

## Material	closed cellular polyether-urethane

S

1500

Colour	orange

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m long

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.05 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 9.21 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 16.66 N/mm² | DIN 53513 (2) |  |
| Static shear modulus (1) | 1.15 N/mm² | DIN 53513 (2) | preload 1.5 N/mm² |
| Dynamic shear modulus (1) | 1.69 N/mm² | DIN 53513 (2) | preload 1.5 N/mm², 10 Hz |
| Resistance to strain | 0.94 N/mm² |  | at 10% deformation |
| Residual compression set | < 8 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 7.0 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 500 % | DIN 53455-6-4 | minimum |
| Tear resistance | > 5.6 N/mm | DIN ISO 34-1/A |  |
| Rebound elasticity | 70 % | DIN EN ISO 8307 | ± 10% |
| Speciic volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.11 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 up to +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inlammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal lammable |

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

## Load deflection curve

2.5

Speciic load [N/mm2]

2.0

1.5

1.0

0.5

0.0

0	2	4	6	8	10	12

### Recording of the 3rd loading; testing between steel plates at room temperature measured with a delection rate of 1% of the thickness per second

Form factor q = 3

Delection [mm]

## Modulus of elasticity

30

Modulus of elasticity [N/mm2]

20

10

0

0.0	0.5	1.0	1.5	2.0	2.5

### Dynamic test: sinusoidal excitation with an oscilla- ting range of ± 0.11 mm at 10 Hz and ± 0.04 mm at 30 Hz

Quasistatic modulus of elasticity:

tangent modulus taken from the load delection curve

Test according to DIN 53513 Form factor q = 3

Speciic load [N/mm²]

## Natural frequency

2.5

Speciic load [N/mm2]

2.0

1.5

1.0

0.5

0.0

0	5	10	15	20	25

### Natural frequency of a single-degree-of-freedom system consisting of a ixed mass and an elastic bearing consisting of Diepolast dyn S 1500 on

a stiff subgrade. Form factor q = 3

Natural frequency [Hz]

1500

D	olast dyn	S

# Prod	t	t	eet

## Correction values varying form factors

### pec ic load 1.50 N/mm², form factor q = 3

Static load range	Deflection

1.7

1.6

1.5

1.4

1.3

1.2

1.1

1.0

0.9

0.3	1	3	10

### Dynamic modulus of elasticity at 10 Hz	Natural frequency

DISCLAIMER:

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast dyn products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certiied testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

| P+S oly eth n-El tomere | K elwe | Telefo | 4 0 44 980-0 | E-M l: nfo@p -poly ret n de |
| --- | --- | --- | --- | --- |
| Gmb o KG | 49356 ephol | Telef | 4 0 44 980-80 | Internet: w w p -poly eth n de |