Catalogue

Celullar rubber

Version: 2017


# Index

[About cellular rubber 4](#_TOC_250001)

[Cellular-rubber materials 5](#_TOC_250000)

EPDM 6

### Sheets

* Strips
* K-profiles
* D- and P-profiles

CR 24

* Sheets
* Strips

NBR 30

* Sheets
* Strips

Silicone 34

* Sheets
* Strips

Polyether 40

Material datasheets 44

* EPDM
* K-profiles
* D- and P-profiles
* CR
* NBR
* Silicone
* Polyether


## About cellular rubber

Cellular rubber, sponge rubber and foam rubber are all classified as foamed elastomers. Cellular rubber can be used for water, air and oil seals. It is often very soft, which also makes it suitable for thermal insulation and sound absorption.

**Cellular rubber** is a structure of closed cells, open cells or semi-closed cells. The primary trademark of cellular-rubber is excellent compression rate and its ability to regain its original shape.

Applications: parts that are often opened and closed or parted from each other, for example windows, doors, shutters or hatches.

**Foam rubber** has an open cell structure and is used in technical applications as well as in everyday items such as sponges and filters. Due to the large cells and open structure, foam rubber has excellent absorbing abilities. Foam rubber equipped with many pores is often used in mattresses, pillows and lining.

**Sponge rubber** is available with open, closed or semi-closed cells. The difference from cellular-rubber is the skin like surface. The cells are smaller than in foam rubber. Sponge rubber is primarily used as sealing.

All foamed elastomers can be produced from natural components as well as synthetic materials such as SBR, CR, NBR and EPDM rubber. It is also possible to make foamed products from high quality materials such as silicon rubber and Viton®.


## Cellular-rubber materials

#### EPDM (Ethylene Propylene Diene Monomer)

EPDM is part of the group of synthetic rubbers or elastomers which are made in the polymerization of ethylene, propylene and diene. EPDM has excellent resistance to ageing, ozone, oxygen, UV-radiation and numerous acids and alkalis. EPDM is highly recommended for outdoor use due to its superior weather resistance. EPDM is also resistant to steam, water, salts and glycol (anti-freeze). Limited use is advised in applications containing mineral oils, grease and fuels. Temperature range -40°C to +90°C, withstanding temporary peaks in temperature up to +130°.

#### CR (Neoprene, Chloroprene)

Neoprene is a synthetic rubber which is achieved after the polymerization of chloroprene. The presence of the chlorine atom improves the chemical resistance making it superior to, for example SBR and natural rubber, and gives the rubber better weather, -heat, -ozone withstanding qualities. Neoprene is a very versatile rubber quality. Besides very good mechanical and elastic qualities, neoprene is also resistant to numerous chemicals. Neoprene has average to good resistance to mineral and synthetic oils, grease and fuels. Neoprene has however poor low temperature flexibility. Temperature range -40°C to +120°C.

#### NBR (Nitrile Butadiene Rubber)

NBR is a synthetic rubber produced from a copolymer of acrylonitrile and 1,3 butadien and is also known as Nitrile, Perbunan, Buna-N and Hycar. In the production of cellular-rubber PVC is added. NBR has excellent resistance to water, oil, fuel and other petroleum products. It is superior to most elastomers in compression set, cold flow and abrasion resistance. NBR possesses a moderate to average resistance to ozone, sunlight, weather, it does not, however, possess good resistance to aromatic oils, halogenated hydrocarbons, ketones, brake fluids or strong acids. Temperature range -40°C to +100°C.

#### Silicone (Vinyl Methyl Silicone –VMQ)

The silicone foam-rubber has excellent resistance to temperature extremes. The material is very soft, has very good stress relaxing properties, it is easy to re-shape. It is self-extinguishing and very durable, even in outdoor-use. Silicone foam-rubber has a very good resistance to sunlight, ozone, oxygen and gases. The silicone foam-rubber possesses good electrical insulation properties, water repellency, does not oxidize and is completely toxin-free. However, it has poor tensile strength, tear, abrasion and steam resistance. Temperature range -70°C to +200°C.

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

EPDM cellular rubber sheeting without self-adhesive layer

quality : EPDM

colour : black

cellular structure : closed execution : without adhesive temperature range : -40oC to +95oC

density : 120 kg/m3 (+/- 20)

hardness shore 00 : 50 (-10/+5) hardness shore A : ca. 10-15

price per m2 (euro)

7,00

9,50

13,00

16,00

19,00

24,50

31,00

37,00

44,00

59,00

72,00

85,00

115,00

145,00

|  |  |  |  |
| --- | --- | --- | --- |
| article code | thickness (mm) | width (mm) | length (mm) |

|  |  |  |  |
| --- | --- | --- | --- |
| 27700002 | 2 | 1000 | 20000 |
| 27700003 | 3 | 1000 | 20000 |
| 27700004 | 4 | 1000 | 20000 |
| 27700005 | 5 | 1000 | 20000 |
| 27700006 | 6 | 1000 | 20000 |
| 27700008 | 8 | 1000 | 20000 |
| 27700010 | 10 | 1000 | 20000 |
| 27700012 | 12 | 1000 | 10000 |
| 27700015 | 15 | 1000 | 10000 |
| 27700020 | 20 | 1000 | 10000 |
| 27700025 | 25 | 1000 | 2000 |
| 27700030 | 30 | 1000 | 2000 |
| 27700040 | 40 | 1000 | 2000 |
| 27700050 | 50 | 1000 | 2000 |

EPDM Cellular rubber sheeting with self-adhesive, black

quality : EPDM

colour : black cellular structure : closed

execution : one side self-adhesive layer temperature range : -40oC to +95oC

density : 120 kg/m3 (+/- 20)

hardness shore 00 : 50 (-10/+5) hardness shore A : ca. 10-15

price per m2 (euro)

14,00

17,00

20,50

23,50

26,50

35,00

42,00

47,00

55,00

67,50

|  |  |  |  |
| --- | --- | --- | --- |
| article code | thickness (mm) | width (mm) | length (mm) |

|  |  |  |  |
| --- | --- | --- | --- |
| 27710002 | 2 | 1000 | 20000 |
| 27710003 | 3 | 1000 | 20000 |
| 27710004 | 4 | 1000 | 20000 |
| 27710005 | 5 | 1000 | 20000 |
| 27710006 | 6 | 1000 | 20000 |
| 27710008 | 8 | 1000 | 20000 |
| 27710010 | 10 | 1000 | 20000 |
| 27710012 | 12 | 1000 | 10000 |
| 27710015 | 15 | 1000 | 10000 |
| 27710020 | 20 | 1000 | 10000 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

EPDM cellular rubber sheeting with self-adhesive layer, white

quality : EPDM

colour : white cellular structure : closed

execution : one side self-adhesive layer temperature range : -40oC to +95oC

density : 120 kg/m3 (+/- 5)

hardness shore 00 : 40 (+/- 5) hardness shore A : ca. 10-15

price per m2 (euro)

22,50

26,00

30,00

32,50

35,00

47,00

58,00

65,00

78,00

90,00

|  |  |  |  |
| --- | --- | --- | --- |
| article code | thickness (mm) | width (mm) | length (mm) |

|  |  |  |  |
| --- | --- | --- | --- |
| 28010002 | 2 | 1000 | 10000 |
| 28010003 | 3 | 1000 | 10000 |
| 28010004 | 4 | 1000 | 10000 |
| 28010005 | 5 | 1000 | 10000 |
| 28010006 | 6 | 1000 | 10000 |
| 28010008 | 8 | 1000 | 10000 |
| 28010010 | 10 | 1000 | 10000 |
| 28010012 | 12 | 1000 | 10000 |
| 28010015 | 15 | 1000 | 10000 |
| 28010020 | 20 | 1000 | 10000 |

EPDM Cellular rubber sheeting with self-adhesive, grey

quality : EPDM

colour : grey

cellular structure : closed

execution : one side self-adhesive layer temperature range : -40oC to +95oC

density : 120 kg/m3 (+/- 5)

hardness shore 00 : 40 (+/- 5) hardness shore A : ca. 10-15

price per m2 (euro)

23,00

26,50

31,00

33,00

36,00

48,00

59,00

66,00

79,00

92,00

|  |  |  |  |
| --- | --- | --- | --- |
| article code | thickness (mm) | width (mm) | length (mm) |

|  |  |  |  |
| --- | --- | --- | --- |
| 28110002 | 2 | 1000 | 10000 |
| 28110003 | 3 | 1000 | 10000 |
| 28110004 | 4 | 1000 | 10000 |
| 28110005 | 5 | 1000 | 10000 |
| 28110006 | 6 | 1000 | 10000 |
| 28110008 | 8 | 1000 | 10000 |
| 28110010 | 10 | 1000 | 10000 |
| 28110012 | 12 | 1000 | 10000 |
| 28110015 | 15 | 1000 | 10000 |
| 28110020 | 20 | 1000 | 10000 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

0,35

0,35

0,40

0,45

0,43

0,43

0,49

0,55

0,42

0,42

0,48

0,54

0,35

0,35

0,40

0,40

0,50

0,43

0,43

0,42

0,42

0,48

0,48

0,60

0,49

0,49

0,61

0,35

0,35

0,40

0,45

0,50

0,43

0,43

0,49

0,55

0,61

0,42

0,42

0,48

0,54

0,60

Self-adhesive EPDM cellular rubber strips



|  |  |  |  |
| --- | --- | --- | --- |
| colour | black | grey | white |

|  |  |  |  |
| --- | --- | --- | --- |
| quality | EPDM | EPDM | EPDM |
| cellular structure | closed | closed | closed |
| execution | one side self-adhesive layer | one side self-adhesive layer | one side self-adhesive layer |
| temperature range | -40°C to +95°C | -40°C to +95°C | -40°C to +95°C |
| density | 120 (+/-20) kg/m3 | 120 (+/-10) kg/m3 | 120 (+/-10) kg/m3 |
| hardness Shore 00 | 50 (-10/+5) | 40 (+/-5) | 40 (+/-5) |
| hardness Shore A | ca. 10-15 | ca. 10-15 | ca. 10-15 |
| roll length (thickness 2 - 12 mm) | 20 meters | 10 meters | 10 meters |
| roll length (thickness 15 - 20 mm) | 10 meters | 10 meters | 10 meters |

|  |  |  |  |
| --- | --- | --- | --- |
|  | black | grey | white |
| width (mm) | thickness (mm) | article code | price per m (euro) | article code | price per m (euro) | article code | price per m (euro) |

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 5 | 2 | 27000502 | 27300502 | 27200502 |  |
| 5 | 3 | 27000503 | 27300503 | 27200503 |  |
| 5 | 4 | 27000504 | 27300504 | 27200504 |  |
| 5 | 5 | 27000505 | 27300505 | 27200505 |  |
|  |  |  |  |  |  |
| 6 | 2 | 27000602 | 27300602 | 27200602 |  |
| 6 | 3 | 27000603 | 27300603 | 27200603 |  |
| 6 | 4 | 27000604 | 27300604 | 27200604 |  |
| 6 | 5 | 27000605 | 27300605 | 27200605 |  |
| 6 | 6 | 27000606 | 27300606 | 27200606 |  |
|  |  |  |  |  |  |
| 7 | 2 | 27000702 | 27300702 | 27200702 |  |
| 7 | 3 | 27000703 | 27300703 | 27200703 |  |
| 7 | 4 | 27000704 | 27300704 | 27200704 |  |
| 7 | 5 | 27000705 | 27300705 | 27200705 |  |
| 7 | 6 | 27000706 | 27300706 | 27200706 |  |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

0,35

0,43

0,42

0,42

0,35

0,40

0,45

0,50

0,55

0,43

0,49

0,55

0,61

0,67

0,48

0,54

0,60

0,66

0,40

0,40

0,49

0,48

0,48

0,54

0,60

0,49

0,72

0,55

0,84

0,61

0,73

0,85

0,45

0,50

0,60

0,70

0,40

0,40

0,45

0,50

0,60

0,70

0,80

0,49

0,48

0,49

0,48

0,55

0,54

0,61

0,60

0,73

0,72

0,85

0,84

0,98

0,96

0,40

0,45

0,50

0,55

0,65

0,75

0,85

0,49

1,00

0,55

0,61

0,67

0,79

0,92

1,04

1,22

0,48

0,60

0,66

0,54

0,78

0,90

1,02

1,20

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
|  |  |  |  |  |
| width (mm) | thickness (mm) |  |  |  |  |
|  |  |  |  |  |  |
| 8 | 2 | 27000802 |  | 27300802 | 27200802 |
| 8 | 3 | 27000803 |  | 27300803 | 27200803 |
| 8 | 4 | 27000804 |  | 27300804 | 27200804 |
| 8 | 5 | 27000805 |  | 27300805 | 27200805 |
| 8 | 6 | 27000806 |  | 27300806 | 27200806 |
| 8 | 8 | 27000808 |  | 27300808 | 27200808 |
|  |  |  |  |  |  |
| 9 | 2 | 27000902 |  | 27300902 | 27200902 |
| 9 | 3 | 27000903 |  | 27300903 | 27200903 |
| 9 | 4 | 27000904 |  | 27300904 | 27200904 |
| 9 | 5 | 27000905 |  | 27300905 | 27200905 |
| 9 | 6 | 27000906 |  | 27300906 | 27200906 |
| 9 | 8 | 27000908 |  | 27300908 | 27200908 |
|  |  |  |  |  |  |
| 10 | 2 | 27001002 |  | 27301002 | 27201002 |
| 10 | 3 | 27001003 |  | 27301003 | 27201003 |
| 10 | 4 | 27001004 |  | 27301004 | 27201004 |
| 10 | 5 | 27001005 |  | 27301005 | 27201005 |
|  |  |  |  |  |  |
|  |  |  |  |  |  |
|  |  |  |  |  |  |
| 10 | 8 | 27001008 |  | 27301008 | 27201008 |
| 10 | 10 | 27001010 |  | 27301010 | 27201010 |
|  |  |  |  |  |  |
| 12 | 2 | 27001202 |  | 27301202 | 27201202 |
| 12 | 3 | 27001203 |  | 27301203 | 27201203 |
| 12 | 4 | 27001204 |  | 27301204 | 27201204 |
| 12 | 5 | 27001205 |  | 27301205 | 27201205 |
| 12 | 6 | 27001206 |  | 27301206 | 27201206 |
| 12 | 8 | 27001208 |  | 27301208 | 27201208 |
|  |  |  |  |  | 27201210 |
| 12 | 10 | 27001210 |  | 27301210 |  |
|  |  |  |  |  |  |
| 12 | 12 | 27001212 |  | 27301212 | 27201212 |



|  |  |  |
| --- | --- | --- |
| black | grey | white |
| article code | price per m (euro) | article code | price per m (euro) | article code | price per m (euro) |

10 6 27001006 27301006 27201006

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

0,45

0,50

0,55

0,60

0,65

0,55

0,54

0,61

0,60

0,67

0,66

0,73

0,72

0,79

0,78

0,85

1,04

1,02

1,00

1,22

1,20

1,15

1,40

1,40

1,71

1,38

1,68

0,50

0,55

0,65

0,75

0,85

1,05

0,61

0,67

0,79

0,92

1,04

1,28

0,60

0,66

0,78

0,90

1,02

1,26

Self-adhesive EPDM cellular rubber strips



|  |  |  |  |
| --- | --- | --- | --- |
| colour | black | grey | white |

|  |  |  |  |
| --- | --- | --- | --- |
| quality | EPDM | EPDM | EPDM |
| cellular structure | closed | closed | closed |
| execution | one side self-adhesive layer | one side self-adhesive layer | one side self-adhesive layer |
| temperature range | -40°C to +95°C | -40°C to +95°C | -40°C to +95°C |
| density | 120 (+/-20) kg/m3 | 120 (+/-10) kg/m3 | 120 (+/-10) kg/m3 |
| hardness Shore 00 | 50 (-10/+5) | 40 (+/-5) | 40 (+/-5) |
| hardness Shore A | ca. 10-15 | ca. 10-15 | ca. 10-15 |
| roll length (thickness 2 - 10 mm) | 20 meters | 10 meters | 10 meters |
| roll length (thickness 12 - 20 mm) | 10 meters | 10 meters | 10 meters |

|  |  |  |  |
| --- | --- | --- | --- |
|  | black | grey | white |
| width (mm) | thickness (mm) | article code | price per m (euro) | article code | price per m (euro) | article code | price per m (euro) |

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| 15 | 2 | 27001502 | 27301502 | 27201502 |
| 15 | 3 | 27001503 | 27301503 | 27201503 |
| 15 | 4 | 27001504 | 27301504 | 27201504 |
| 15 | 5 | 27001505 | 27301505 | 27201505 |
| 15 | 6 | 27001506 | 27301506 | 27201506 |
| 15 | 8 | 27001508 | 27301508 | 27201508 |
| 15 | 10 | 27001510 | 27301510 | 27201510 |
| 15 | 12 | 27001512 | 27301512 | 27201512 |
| 15 | 15 | 27001515 | 27301515 | 27201515 |
|  |  |  |  |  |
| 18 | 2 | 27001802 | 27301802 | 27201802 |
| 18 | 3 | 27001803 | 27301803 | 27201803 |
| 18 | 4 | 27001804 | 27301804 | 27201804 |
| 18 | 5 | 27001805 | 27301805 | 27201805 |
| 18 | 6 | 27001806 | 27301806 | 27201806 |
| 18 | 8 | 27001808 | 27301808 | 27201808 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

1,20

1,65

1,85

1,46

1,44

1,98

2,22

2,01

2,26

0,50

0,61

0,60

0,60

0,73

0,72

0,70

0,85

0,84

0,80

0,98

0,96

0,90

1,10

1,08

1,10

1,34

1,32

1,25

1,53

1,50

3,10

3,78

3,72

0,70

0,90

1,05

1,15

0,85

0,84

1,08

1,10

1,28

1,26

1,30

1,40

1,38

1,50

1,59

1,56

1,90

1,83

1,80

2,28

2,32

2,58

3,06

4,20

2,62

3,11

4,27

2,15

2,55

3,50

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
|  |  | black | grey | white |
| width (mm) | thickness (mm) | article code | price per m (euro) | article code | price per m (euro) | article code | price per m (euro) |
|  |  |  |  |  |
| 18 | 10 | 27001810 | 27301810 | 27201810 |
| 18 | 12 | 27001812 | 27301812 | 27201812 |
| 18 | 15 | 27001815 | 27301815 | 27201815 |
|  |  |  |  |  |
| 20 | 2 | 27002002 | 27302002 | 27202002 |
| 20 | 3 | 27002003 | 27302003 | 27202003 |
| 20 | 4 | 27002004 | 27302004 | 27202004 |
| 20 | 5 | 27002005 | 27302005 | 27202005 |
| 20 | 6 | 27002006 | 27302006 | 27202006 |
| 20 | 8 | 27002008 | 27302008 | 27202008 |
| 20 | 10 | 27002010 | 27302010 | 27202010 |
| 20 | 12 | 27002012 | 27302012 | 27202012 |
| 20 | 15 | 27002015 | 27302015 | 27202015 |
| 20 | 20 | 27002020 | 27302020 | 27202020 |
|  |  |  |  |  |
| 25 | 2 | 27002502 | 27302502 | 27202502 |
| 25 | 3 | 27002503 | 27302503 | 27202503 |
|  |  |  |  |  |
|  |  |  |  |  |
|  |  |  |  |  |
| 25 | 5 | 27002505 | 27302505 | 27202505 |
| 25 | 6 | 27002506 | 27302506 | 27202506 |
| 25 | 8 | 27002508 | 27302508 | 27202508 |
| 25 | 10 | 27002510 | 27302510 | 27202510 |
| 25 | 12 | 27002512 | 27302512 | 27202512 |
| 25 | 15 | 27002515 | 27302515 | 27202515 |
| 25 | 20 | 27002520 | 27302520 | 27202520 |
|  |  |  |  |  |
| 30 | 2 | 27003002 | 27303002 | 27203002 |
| 30 | 3 | 27003003 | 27303003 | 27203003 |
| 30 | 4 | 27003004 | 27303004 | 27203004 |
| 30 | 5 | 27003005 | 27303005 | 27203005 |
| 30 | 6 | 27003006 | 27303006 | 27203006 |
| 30 | 8 | 27003008 | 27303008 | 27203008 |
| 30 | 10 | 27003010 | 27303010 | 27203010 |
| 30 | 12 | 27003012 | 27303012 | 27203012 |
| 30 | 15 | 27003015 | 27303015 | 27203015 |
| 30 | 20 | 27003020 | 27303020 | 27203020 |



25 4 27002504 27302504 27202504

2,04

2,28

3,12

2,07

3,17

2,32

1,70

1,90

2,60

0,65

0,80

0,79

0,98

0,78

0,96

1,08

1,10

0,90

1,00

1,22

1,20

1,15

1,40

1,38

1,35

1,65

1,62

1,75

2,14

2,10

1,85

2,25

2,22

2,20

2,68

2,64

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

0,85

1,04

1,02

1,26

1,44

1,62

1,80

2,10

2,58

3,12

3,54

4,86

1,28

1,46

1,65

1,83

2,14

2,62

3,17

3,60

4,94

1,05

1,20

1,35

1,50

1,75

2,15

2,60

2,95

4,05

0,95

1,16

1,14

1,15

1,30

1,55

1,70

2,00

1,40

1,59

1,89

2,07

2,44

1,38

1,56

1,86

2,04

2,40

Self-adhesive EPDM cellular rubber strips



|  |  |  |  |
| --- | --- | --- | --- |
| colour | black | grey | white |

|  |  |  |  |
| --- | --- | --- | --- |
| quality | EPDM | EPDM | EPDM |
| cellular structure | closed | closed | closed |
| execution | one side self-adhesive layer | one side self-adhesive layer | one side self-adhesive layer |
| temperature range | -40°C to +95°C | -40°C to +95°C | -40°C to +95°C |
| density | 120 (+/-20) kg/m3 | 120 (+/-10) kg/m3 | 120 (+/-10) kg/m3 |
| hardness Shore 00 | 50 (-10/+5) | 40 (+/-5) | 40 (+/-5) |
| hardness Shore A | ca. 10-15 | ca. 10-15 | ca. 10-15 |
| roll length (thickness 2 - 12 mm) | 20 meters | 10 meters | 10 meters |
| roll length (thickness 15 - 20 mm) | 10 meters | 10 meters | 10 meters |

|  |  |  |  |
| --- | --- | --- | --- |
|  | black | grey | white |
| width (mm) | thickness (mm) | article code | price per m (euro) | article code | price per m (euro) | article code | price per m (euro) |

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| 35 | 2 | 27003502 | 27303502 | 27203502 |
| 35 | 3 | 27003503 | 27303503 | 27203503 |
| 35 | 4 | 27003504 | 27303504 | 27203504 |
| 35 | 5 | 27003505 | 27303505 | 27203505 |
| 35 | 6 | 27003506 | 27303506 | 27203506 |
| 35 | 8 | 27003508 | 27303508 | 27203508 |
| 35 | 10 | 27003510 | 27303510 | 27203510 |
| 35 | 12 | 27003512 | 27303512 | 27203512 |
| 35 | 15 | 27003515 | 27303515 | 27203515 |
| 35 | 20 | 27003520 | 27303520 | 27203520 |
|  |  |  |  |  |
| 40 | 2 | 27004002 | 27304002 | 27204002 |
| 40 | 3 | 27004003 | 27304003 | 27204003 |
| 40 | 4 | 27004004 | 27304004 | 27204004 |
| 40 | 5 | 27004005 | 27304005 | 27204005 |
| 40 | 6 | 27004006 | 27304006 | 27204006 |
| 40 | 8 | 27004008 | 27304008 | 27204008 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

3,05

3,30

4,55

2,87

3,72

4,03

5,55

2,82

3,66

3,96

1,10

1,30

1,75

2,00

2,25

2,60

3,15

3,85

4,40

5,75

1,34

1,59

2,14

2,44

2,75

1,32

1,56

2,10

2,40

2,70

3,12

3,17

3,78

4,62

5,28

6,90

3,84

4,70

5,37

7,02

1,40

1,71

1,68

1,80

2,20

2,16

2,10

2,56

2,52

2,30

2,81

2,76

2,60

3,17

3,12

3,00

3,80

4,30

5,10

7,00

3,66

4,64

5,25

6,22

8,54

3,60

4,56

5,16

6,12

8,40

1,65

2,01

1,98

2,46

2,50

2,05

2,35

2,70

2,87

2,82

3,24

3,60

4,20

5,10

6,24

7,02

9,60

3,00

3,50

4,25

5,20

5,85

8,00

3,29

3,66

4,27

5,19

6,34

7,14

9,76

70

20

27007020

27307020

27207020

|  |  |  |
| --- | --- | --- |
| black | grey | white |
| article code | price per m (euro) | article code | price per m (euro) | article code | price per m (euro) |



|  |  |  |  |  |
| --- | --- | --- | --- | --- |
|  |  |  |  |  |
| width (mm) | thickness (mm) |  |  |  |  |
|  |  |  |  |  |  |
| 40 | 10 | 27004010 | 27304010 |  | 27204010 |
| 40 | 12 | 27004012 | 27304012 |  | 27204012 |
| 40 | 15 | 27004015 | 27304015 |  | 27204015 |
| 40 | 20 | 27004020 | 27304020 |  | 27204020 |
|  |  |  |  |  |  |
| 50 | 2 | 27005002 | 27305002 |  | 27205002 |
| 50 | 3 | 27005003 | 27305003 |  | 27205003 |
| 50 | 4 | 27005004 | 27305004 |  | 27205004 |
| 50 | 5 | 27005005 | 27305005 |  | 27205005 |
| 50 | 6 | 27005006 | 27305006 |  | 27205006 |
| 50 | 8 | 27005008 | 27305008 |  | 27205008 |
| 50 | 10 | 27005010 | 27305010 |  | 27205010 |
| 50 | 12 | 27005012 | 27305012 |  | 27205012 |
| 50 | 15 | 27005015 | 27305015 |  | 27205015 |
| 50 | 20 | 27005020 | 27305020 |  | 27205020 |
|  |  |  |  |  |  |
| 60 | 2 | 27006002 | 27306002 |  | 27206002 |
| 60 | 3 | 27006003 | 27306003 |  | 27206003 |
| 60 | 4 | 27006004 | 27306004 |  | 27206004 |
| 60 | 5 | 27006005 | 27306005 |  | 27206005 |
| 60 | 6 | 27006006 | 27306006 |  | 27206006 |
| 60 | 8 | 27006008 | 27306008 |  | 27206008 |
| 60 | 10 | 27006010 | 27306010 |  | 27206010 |
| 60 | 12 | 27006012 | 27306012 |  | 27206012 |
| 60 | 15 | 27006015 | 27306015 |  | 27206015 |
| 60 | 20 | 27006020 | 27306020 |  | 27206020 |
|  |  |  |  |  |  |
| 70 | 2 | 27007002 | 27307002 |  | 27207002 |
| 70 | 3 | 27007003 | 27307003 |  | 27207003 |
| 70 | 4 | 27007004 | 27307004 |  | 27207004 |
| 70 | 5 | 27007005 | 27307005 |  | 27207005 |
| 70 | 6 | 27007006 | 27307006 |  | 27207006 |
| 70 | 8 | 27007008 | 27307008 |  | 27207008 |
| 70 | 10 | 27007010 | 27307010 |  | 27207010 |
| 70 | 12 | 27007012 | 27307012 |  | 27207012 |
| 70 | 15 | 27007015 | 27307015 |  | 27207015 |
|  |  |  |  |  |  |
|  |  |  |  |  |  |
|  |  |  |  |  |  |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

1,75

2,14

2,10

2,10

2,65

3,00

3,40

3,95

4,90

5,70

6,60

8,85

2,56

3,23

3,66

4,15

4,82

5,98

6,95

8,05

10,80

2,52

3,18

3,60

4,08

4,74

5,88

6,84

7,92

10,62

Self-adhesive EPDM cellular rubber strips



|  |  |  |  |
| --- | --- | --- | --- |
| colour | black | grey | white |

|  |  |  |  |
| --- | --- | --- | --- |
| quality | EPDM | EPDM | EPDM |
| cellular structure | closed | closed | closed |
| execution | one side self-adhesive layer | one side self-adhesive layer | one side self-adhesive layer |
| temperature range | -40°C to +95°C | -40°C to +95°C | -40°C to +95°C |
| density | 120 (+/-20) kg/m3 | 120 (+/-10) kg/m3 | 120 (+/-10) kg/m3 |
| hardness Shore 00 | 50 (-10/+5) | 40 (+/-5) | 40 (+/-5) |
| hardness Shore A | ca. 10-15 | ca. 10-15 | ca. 10-15 |
| roll length (thickness 2 - 12 mm) | 20 meters | 10 meters | 10 meters |
| roll length (thickness 15 - 20 mm) | 10 meters | 10 meters | 10 meters |

|  |  |  |  |
| --- | --- | --- | --- |
|  | black | grey | white |
| width (mm) | thickness (mm) | article code | price per m (euro) | article code | price per m (euro) | article code | price per m (euro) |

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| 75 | 2 | 27007502 | 27307502 | 27207502 |
| 75 | 3 | 27007503 | 27307503 | 27207503 |
| 75 | 4 | 27007504 | 27307504 | 27207504 |
| 75 | 5 | 27007505 | 27307505 | 27207505 |
| 75 | 6 | 27007506 | 27307506 | 27207506 |
| 75 | 8 | 27007508 | 27307508 | 27207508 |
| 75 | 10 | 27007510 | 27307510 | 27207510 |
| 75 | 12 | 27007512 | 27307512 | 27207512 |
| 75 | 15 | 27007515 | 27307515 | 27207515 |
| 75 | 20 | 27007520 | 27307520 | 27207520 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

1,90

2,30

2,80

2,32

2,28

2,76

2,81

3,36

3,42

3,10

3,40

3,78

3,72

4,08

4,15

4,80

4,88

4,00

5,00

6,10

6,00

6,10

6,55

9,10

7,44

7,99

11,10

7,32

7,86

10,92

2,05

2,45

3,05

3,50

3,90

2,50

2,46

2,94

3,66

2,99

3,72

4,27

4,76

4,20

4,68

5,52

6,60

8,22

9,24

12,36

5,61

6,71

8,36

9,39

12,57

4,60

5,50

6,85

7,70

10,30

2,20

2,68

2,64

3,12

3,17

4,20

2,60

3,50

4,27

4,80

4,00

4,88

5,40

4,50

5,49

6,24

7,56

9,24

6,34

5,20

6,30

7,70

8,80

11,50

7,69

9,39

10,74

14,03

10,56

13,80



|  |  |  |  |  |
| --- | --- | --- | --- | --- |
|  |  | black | grey | white |
| width (mm) | thickness (mm) | article code | price per m (euro) | article code | price per m (euro) | article code | price per m (euro) |
|  |  |  |  |  |
| 80 | 2 | 27008002 | 27308002 | 27208002 |
| 80 | 3 | 27008003 | 27308003 | 27208003 |
| 80 | 4 | 27008004 | 27308004 | 27208004 |
| 80 | 5 | 27008005 | 27308005 | 27208005 |
| 80 | 6 | 27008006 | 27308006 | 27208006 |
| 80 | 8 | 27008008 | 27308008 | 27208008 |
| 80 | 10 | 27008010 | 27308010 | 27208010 |
| 80 | 12 | 27008012 | 27308012 | 27208012 |
| 80 | 15 | 27008015 | 27308015 | 27208015 |
| 80 | 20 | 27008020 | 27308020 | 27208020 |
|  |  |  |  |  |
| 90 | 2 | 27009002 | 27309002 | 27209002 |
| 90 | 3 | 27009003 | 27309003 | 27209003 |
| 90 | 4 | 27009004 | 27309004 | 27209004 |
| 90 | 5 | 27009005 | 27309005 | 27209005 |
| 90 | 6 | 27009006 | 27309006 | 27209006 |
| 90 | 8 | 27009008 | 27309008 | 27209008 |
| 90 | 10 | 27009010 | 27309010 | 27209010 |
| 90 | 12 | 27009012 | 27309012 | 27209012 |
| 90 | 15 | 27009015 | 27309015 | 27209015 |
| 90 | 20 | 27009020 | 27309020 | 27209020 |
|  |  |  |  |  |
| 100 | 2 | 27010002 | 27310002 | 27210002 |
| 100 | 3 | 27010003 | 27310003 | 27210003 |
| 100 | 4 | 27010004 | 27310004 | 27210004 |
| 100 | 5 | 27010005 | 27310005 | 27210005 |
| 100 | 6 | 27010006 | 27310006 | 27210006 |
| 100 | 8 | 27010008 | 27310008 | 27210008 |
| 100 | 10 | 27010010 | 27310010 | 27210010 |
| 100 | 12 | 27010012 | 27310012 | 27210012 |
| 100 | 15 | 27010015 | 27310015 | 27210015 |
| 100 | 20 | 27010020 | 27310020 | 27210020 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

3,30

4,03

3,96

4,68

6,30

7,20

4,76

6,41

8,10

9,36

7,32

8,24

11,34

9,52

13,86

15,84

20,70

11,53

14,09

16,10

21,05

3,90

5,25

6,00

6,75

7,80

9,45

11,55

13,20

17,25

Self-adhesive EPDM cellular rubber strips



|  |  |  |  |
| --- | --- | --- | --- |
| colour | black | grey | white |

|  |  |  |  |
| --- | --- | --- | --- |
| quality | EPDM | EPDM | EPDM |
| cellular structure | closed | closed | closed |
| execution | one side self-adhesive layer | one side self-adhesive layer | one side self-adhesive layer |
| temperature range | -40°C to +95°C | -40°C to +95°C | -40°C to +95°C |
| density | 120 (+/-20) kg/m3 | 120 (+/-10) kg/m3 | 120 (+/-10) kg/m3 |
| hardness Shore 00 | 50 (-10/+5) | 40 (+/-5) | 40 (+/-5) |
| hardness Shore A | ca. 10-15 | ca. 10-15 | ca. 10-15 |
| roll length (thickness 2 - 12 mm) | 20 meters | 10 meters | 10 meters |
| roll length (thickness 15 - 20 mm) | 10 meters | 10 meters | 10 meters |

|  |  |  |  |
| --- | --- | --- | --- |
|  | black | grey | white |
| width (mm) | thickness (mm) | article code | price per m (euro) | article code | price per m (euro) | article code | price per m (euro) |

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| 150 | 2 | 27015002 | 27315002 | 27215002 |
| 150 | 3 | 27015003 | 27315003 | 27215003 |
| 150 | 4 | 27015004 | 27315004 | 27215004 |
| 150 | 5 | 27015005 | 27315005 | 27215005 |
| 150 | 6 | 27015006 | 27315006 | 27215006 |
| 150 | 8 | 27015008 | 27315008 | 27215008 |
| 150 | 10 | 27015010 | 27315010 | 27215010 |
| 150 | 12 | 27015012 | 27315012 | 27215012 |
| 150 | 15 | 27015015 | 27315015 | 27215015 |
| 150 | 20 | 27015020 | 27315020 | 27215020 |

4,40

5,20

5,37

5,28

6,34

6,24

7,00

8,54

8,40

9,60

10,80

12,48

8,00

9,76

9,00

10,98

15,12

10,40

12,69

12,60

15,37

15,40

17,60

23,00

18,79

21,47

28,06

18,48

21,12

27,60

5,50

6,71

6,60

6,50

7,93

7,80

8,75

10,68

10,50

10,00

12,20

12,00

11,25

13,00

15,75

19,25

22,00

28,75

13,73

15,86

19,22

23,49

26,84

35,08

13,50

15,60

18,90

23,10

26,40

34,50

6,60

8,05

7,92

7,80

9,52

9,36

10,50

12,81

12,60

12,00

13,50

15,60

18,90

23,10

26,40

34,50

14,64

16,47

19,03

23,06

28,18

32,21

42,09

14,40

16,20

18,72

22,68

27,72

31,68

41,40



|  |  |  |  |  |
| --- | --- | --- | --- | --- |
|  |  | black | grey | white |
| width (mm) | thickness (mm) | article code | price per m (euro) | article code | price per m (euro) | article code | price per m (euro) |
|  |  |  |  |  |
| 200 | 2 | 27020002 | 27320002 | 27220002 |
| 200 | 3 | 27020003 | 27320003 | 27220003 |
| 200 | 4 | 27020004 | 27320004 | 27220004 |
| 200 | 5 | 27020005 | 27320005 | 27220005 |
| 200 | 6 | 27020006 | 27320006 | 27220006 |
| 200 | 8 | 27020008 | 27320008 | 27220008 |
| 200 | 10 | 27020010 | 27320010 | 27220010 |
| 200 | 12 | 27020012 | 27320012 | 27220012 |
| 200 | 15 | 27020015 | 27320015 | 27220015 |
| 200 | 20 | 27020020 | 27320020 | 27220020 |
|  |  |  |  |  |
| 250 | 2 | 27025002 | 27325002 | 27225002 |
| 250 | 3 | 27025003 | 27325003 | 27225003 |
| 250 | 4 | 27025004 | 27325004 | 27225004 |
| 250 | 5 | 27025005 | 27325005 | 27225005 |
| 250 | 6 | 27025006 | 27325006 | 27225006 |
| 250 | 8 | 27025008 | 27325008 | 27225008 |
| 250 | 10 | 27025010 | 27325010 | 27225010 |
| 250 | 12 | 27025012 | 27325012 | 27225012 |
| 250 | 15 | 27025015 | 27325015 | 27225015 |
| 250 | 20 | 27025020 | 27325020 | 27225020 |
|  |  |  |  |  |
| 300 | 2 | 27030002 | 27330002 | 27230002 |
| 300 | 3 | 27030003 | 27330003 | 27230003 |
| 300 | 4 | 27030004 | 27330004 | 27230004 |
| 300 | 5 | 27030005 | 27330005 | 27230005 |
| 300 | 6 | 27030006 | 27330006 | 27230006 |
| 300 | 8 | 27030008 | 27330008 | 27230008 |
| 300 | 10 | 27030010 | 27330010 | 27230010 |
| 300 | 12 | 27030012 | 27330012 | 27230012 |
| 300 | 15 | 27030015 | 27330015 | 27230015 |
| 300 | 20 | 27030020 | 27330020 | 27230020 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

8,80

10,40

14,00

16,00

18,00

20,80

25,20

30,80

35,20

46,00

10,74

12,69

17,08

19,52

21,96

25,38

30,74

37,58

42,94

56,12

10,56

12,48

16,80

19,20

21,60

24,96

30,24

36,96

42,24

55,20

Self-adhesive EPDM cellular rubber strips



|  |  |  |  |
| --- | --- | --- | --- |
| colour | black | grey | white |

|  |  |  |  |
| --- | --- | --- | --- |
| quality | EPDM | EPDM | EPDM |
| cellular structure | closed | closed | closed |
| execution | one side self-adhesive layer | one side self-adhesive layer | one side self-adhesive layer |
| temperature range | -40°C to +95°C | -40°C to +95°C | -40°C to +95°C |
| density | 120 (+/-20) kg/m3 | 120 (+/-10) kg/m3 | 120 (+/-10) kg/m3 |
| hardness Shore 00 | 50 (-10/+5) | 40 (+/-5) | 40 (+/-5) |
| hardness Shore A | ca. 10-15 | ca. 10-15 | ca. 10-15 |
| roll length (thickness 2 - 12 mm) | 20 meters | 10 meters | 10 meters |
| roll length (thickness 15 - 20 mm) | 10 meters | 10 meters | 10 meters |

|  |  |  |  |
| --- | --- | --- | --- |
|  | black | grey | white |
| width (mm) | thickness (mm) | article code | price per m (euro) | article code | price per m (euro) | article code | price per m (euro) |

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| 400 | 2 | 27040002 | 27340002 | 27240002 |
| 400 | 3 | 27040003 | 27340003 | 27240003 |
| 400 | 4 | 27040004 | 27340004 | 27240004 |
| 400 | 5 | 27040005 | 27340005 | 27240005 |
| 400 | 6 | 27040006 | 27340006 | 27240006 |
| 400 | 8 | 27040008 | 27340008 | 27240008 |
| 400 | 10 | 27040010 | 27340010 | 27240010 |
| 400 | 12 | 27040012 | 27340012 | 27240012 |
| 400 | 15 | 27040015 | 27340015 | 27240015 |
| 400 | 20 | 27040020 | 27340020 | 27240020 |

11,00

13,00

17,50

20,00

13,42

13,20

15,86

21,35

15,60

21,00

24,00

22,50

26,00

31,50

38,50

44,00

57,50

24,40

27,45

31,72

38,43

46,97

53,68

70,15

27,00

31,20

37,80

46,20

52,80

69,00

11,88

14,04

18,90

21,60

24,30

14,49

17,13

23,06

14,26

16,85

22,68

26,35

25,92

29,16

29,65

28,08

33,70

40,82

49,90

57,02

74,52

34,26

41,50

50,73

57,97

75,76

34,02

41,58

47,52

62,10

12,94

15,29

20,58

23,52

26,46

30,58

45,28

51,74

67,62

15,78

18,65

15,52

18,35

25,11

28,69

32,28

24,70

28,22

37,30

45,19

55,24

63,12

82,50

31,75

36,69

44,45

54,34

62,09

81,14



|  |  |  |  |  |
| --- | --- | --- | --- | --- |
|  |  | black | grey | white |
| width (mm) | thickness (mm) | article code | price per m (euro) | article code | price per m (euro) | article code | price per m (euro) |
|  |  |  |  |  |
| 500 | 2 | 27050002 | 27350002 | 27250002 |
| 500 | 3 | 27050003 | 27350003 | 27250003 |
| 500 | 4 | 27050004 | 27350004 | 27250004 |
| 500 | 5 | 27050005 | 27350005 | 27250005 |
| 500 | 6 | 27050006 | 27350006 | 27250006 |
| 500 | 8 | 27050008 | 27350008 | 27250008 |
| 500 | 10 | 27050010 | 27350010 | 27250010 |
| 500 | 12 | 27050012 | 27350012 | 27250012 |
| 500 | 15 | 27050015 | 27350015 | 27250015 |
| 500 | 20 | 27050020 | 27350020 | 27250020 |
|  |  |  |  |  |
| 600 | 2 | 27060002 | 27360002 | 27260002 |
| 600 | 3 | 27060003 | 27360003 | 27260003 |
| 600 | 4 | 27060004 | 27360004 | 27260004 |
| 600 | 5 | 27060005 | 27360005 | 27260005 |
| 600 | 6 | 27060006 | 27360006 | 27260006 |
| 600 | 8 | 27060008 | 27360008 | 27260008 |
| 600 | 10 | 27060010 | 27360010 | 27260010 |
| 600 | 12 | 27060012 | 27360012 | 27260012 |
| 600 | 15 | 27060015 | 27360015 | 27260015 |
| 600 | 20 | 27060020 | 27360020 | 27260020 |
|  |  |  |  |  |
| 700 | 2 | 27070002 | 27370002 | 27270002 |
| 700 | 3 | 27070003 | 27370003 | 27270003 |
| 700 | 4 | 27070004 | 27370004 | 27270004 |
| 700 | 5 | 27070005 | 27370005 | 27270005 |
| 700 | 6 | 27070006 | 27370006 | 27270006 |
| 700 | 8 | 27070008 | 27370008 | 27270008 |
| 700 | 10 | 27070010 | 27370010 | 27270010 |
| 700 | 12 | 27070012 | 27370012 | 27270012 |
| 700 | 15 | 27070015 | 27370015 | 27270015 |
| 700 | 20 | 27070020 | 27370020 | 27270020 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

13,53

15,99

21,53

24,60

27,68

31,98

38,75

47,36

54,12

65,00

16,51

19,51

26,26

30,01

33,76

39,02

47,27

57,78

66,03

79,30

16,24

19,19

25,83

29,52

33,21

38,38

46,49

56,83

64,94

78,00

Self-adhesive EPDM cellular rubber strips



|  |  |  |  |
| --- | --- | --- | --- |
| colour | black | grey | white |

|  |  |  |  |
| --- | --- | --- | --- |
| quality | EPDM | EPDM | EPDM |
| cellular structure | closed | closed | closed |
| execution | one side self-adhesive layer | one side self-adhesive layer | one side self-adhesive layer |
| temperature range | -40°C to +95°C | -40°C to +95°C | -40°C to +95°C |
| density | 120 (+/-20) kg/m3 | 120 (+/-10) kg/m3 | 120 (+/-10) kg/m3 |
| hardness Shore 00 | 50 (-10/+5) | 40 (+/-5) | 40 (+/-5) |
| hardness Shore A | ca. 10-15 | ca. 10-15 | ca. 10-15 |
| roll length (thickness 2 - 12 mm) | 20 meters | 10 meters | 10 meters |
| roll length (thickness 15 - 20 mm) | 10 meters | 10 meters | 10 meters |

|  |  |  |  |
| --- | --- | --- | --- |
|  | black | grey | white |
| width (mm) | thickness (mm) | article code | price per m (euro) | article code | price per m (euro) | article code | price per m (euro) |

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| 750 | 2 | 27075002 | 27375002 | 27275002 |
| 750 | 3 | 27075003 | 27375003 | 27275003 |
| 750 | 4 | 27075004 | 27375004 | 27275004 |
| 750 | 5 | 27075005 | 27375005 | 27275005 |
| 750 | 6 | 27075006 | 27375006 | 27275006 |
| 750 | 8 | 27075008 | 27375008 | 27275008 |
| 750 | 10 | 27075010 | 27375010 | 27275010 |
| 750 | 12 | 27075012 | 27375012 | 27275012 |
| 750 | 15 | 27075015 | 27375015 | 27275015 |
| 750 | 20 | 27075020 | 27375020 | 27275020 |



## Sponge rubber K-profile

K-profile is a sponge rubber self-adhesive sealing strip made out of high quality and long lasting EPDM rubber, specially designed for windows and doors. The glass fibre reinforced tape on the back of the profile facilitates the installation.

The K-profile is suitable for indoor as well as outdoor applications and has a temperature range from -50°C to

+90°C. Lowest recommended installation temperature is +5°C combined with a 25% compression.

**Applications:** Wooden frames, factory glazing, windows and doors



EPDM sponge rubber K-profile

quality : EPDM

colour : black

celstucture : closed

execution : one side self-adhesive layer temperature range : -50°C to +90°C

density : 350 kg/m3 (+/- 50)

hardness shore 00 : ca. 45 hardness shore A : ca. 10 min. compression : 25%

price per meter (euro)

0,50

0,60

0,75

0,95

0,82

1,10

0,98

|  |  |  |  |
| --- | --- | --- | --- |
| article code | width (mm) | thickness (mm) | roll length (m) |

|  |  |  |  |
| --- | --- | --- | --- |
| 26801415 | 8 | 2 | 225 |
| 26801422 | 9 | 4 | 125 |
| 26801428 | 10 | 5 | 100 |
| 26801432 | 10 | 6 | 75 |
| 26801440 | 15 | 3 | 100 |
| 26801448 | 15 | 8 | 50 |
| 26801458 | 20 | 4 | 50 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.


## D-profiles

The D-profiles are produced from high quality EPDM sponge rubber with closed cells. The D-shaped tunnel gives the profile a high compression and a strong recovery ability, resulting in a durable seal.

The profile is equipped with a self-adhesive layer, reinforced with glass fibre, preventing over-stretching in the installation.

The D-profile can be used indoors as well as outdoors, with a temperature range from -50°C to +90°C. Lowest recommended installation temperature is +5°C.

**Applications:** Air and water tight seals in window and door frames



#### EPDM D-profiles

quality : EPDM

colour : black

celstucture : closed

execution : one side self-adhesive layer temperature range : -50°C to +90°C

density : 350 kg/m3 (+/- 50)

hardness shore 00 : ca. 45 hardness shore A : ca. 10 min. compression : 25%

price per m (euro)

0,80

1,60

4,80

7,00

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| article code | width (mm) | thickness (mm) | colour | roll length (m) |
| 26801206 | 6 | 8 | black | 100 |
| 26801210 | 10 | 12 | black | 70 (2x35) |
| 26801810 | 18 | 10 | black | 25 |
| 26802020 | 20 | 20 | black | 25 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.


## P-profiles

The P-profile is produced in high quality rubber from extruded EPDM with closed cells. The circle shaped air tunnel allows the profile to compress with ease, this makes excellent sealing and filling properties. The strong self-adhesive layer is reinforced with a fine glass fibre mesh, which allows movement without excessive stretching.

The P-profile can be used outdoors as well as indoors with a temperature range from -50°C to +90C. Lowest recommended installation temperature is +5°C.

**Applications:** Filling and sealing gaps in for example door and window frames.



#### EPDM P-profiles

quality : EPDM

celstucture : closed

execution : one side self-adhesive layer temperature range : -50°C to +90°C

density : 350 kg/m3 (-100/+50) hardness shore 00 : ca. 45

hardness shore A : ca. 10 min. compression : 25%

price per m (euro)

0,70

0,95

0,95

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| article code | width (mm) | thickness (mm) | colour | roll length (m) |
| 26801010 | 9 | 5,5 | black | 100 (2x50) |
| 26801010W | 9 | 5,5 | white | 100 (2x50) |
| 26801010B | 9 | 5,5 | bruin | 100 (2x50) |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

CR cellular rubber sheeting without adhesive

quality : CR

colour : black cellular structure : closed

execution : without adhesive temperature range : -40°C to +120°C density : 150 kg/m3 (+/-25) hardness shore 00 : 50 (+/- 5) hardness shore A : ca. 10-15

price per m2 (euro)

8,50

13,00

17,00

20,00

24,00

33,00

40,00

60,00

80,00

100,00

120,00

160,00

180,00

280,00

350,00

460,00

|  |  |  |  |
| --- | --- | --- | --- |
| article code | thickness (mm) | width (mm) | length (mm) |

|  |  |  |  |
| --- | --- | --- | --- |
| 27800002 | 2 | 1000 | 20000 |
| 27800003 | 3 | 1000 | 20000 |
| 27800004 | 4 | 1000 | 20000 |
| 27800005 | 5 | 1000 | 20000 |
| 27800006 | 6 | 1000 | 20000 |
| 27800008 | 8 | 1000 | 20000 |
| 27800010 | 10 | 1000 | 20000 |
| 27800015 | 15 | 1000 | 10000 |
| 27800020 | 20 | 1000 | 2000 |
| 27800025 | 25 | 1000 | 2000 |
| 27800030 | 30 | 1000 | 2000 |
| 27800040 | 40 | 1000 | 2000 |
| 27800050 | 50 | 1000 | 2000 |
| 27800060 | 60 (\*) | 1000 | 2000 |
| 27800080 | 80 (\*\*) | 1000 | 2000 |
| 27800100 | 100 (\*\*\*) | 1000 | 2000 |

Additional information:

(\*) this is 2 x 30mm glued (\*\*) this is 2 x 40mm glued (\*\*\*) this is 2 x 50mm glued

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

Self-adhesive CR cellular rubber sheeting

quality : CR

colour : black cellular structure : closed

execution : one side self-adhesive layer temperature range : -40°C to +120°C

density : 150 kg/m3 (+/-25) hardness shore 00 : 50 (+/- 5) hardness shore A : ca. 10-15

price per m2 (euro)

18,00

23,00

28,00

32,50

37,00

47,00

58,00

61,00

85,00

105,00

|  |  |  |  |
| --- | --- | --- | --- |
| article code | thickness (mm) | width (mm) | length (mm) |

|  |  |  |  |
| --- | --- | --- | --- |
| 27810002 | 2 | 1000 | 20000 |
| 27810003 | 3 | 1000 | 20000 |
| 27810004 | 4 | 1000 | 20000 |
| 27810005 | 5 | 1000 | 20000 |
| 27810006 | 6 | 1000 | 20000 |
| 27810008 | 8 | 1000 | 20000 |
| 27810010 | 10 | 1000 | 20000 |
| 27810012 | 12 | 1000 | 10000 |
| 27810015 | 15 | 1000 | 10000 |
| 27810020 | 20 | 1000 | 10000 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

Self-adhesive CR cellular rubber strips

colour : black

cellular structure : closed

execution : one side self-adhesive layer

temperature range : -40°C to +120°C

density : 150 Kg/m3 (+/- 25)

hardness Shore 00 : 50 (+/- 5)

hardness Shore A : ca. 10 - 15 roll length (thickness 2-12 mm) : 20 meters roll length (thickness 15-20 mm) : 10 meters

price per m (euro)

0,44

0,44

0,50

0,56

0,44

0,44

0,50

0,50

0,63

0,44

0,44

0,50

0,56

0,63

0,44

0,44

0,50

0,56

0,63

0,69

0,50

0,50

0,56

0,63

0,75

0,88

0,50

0,50

0,56

0,63

0,75

0,88

1,00

price per m (euro)

0,50

0,56

0,63

0,69

0,81

0,94

1,06

1,25

0,56

0,63

0,69

0,75

0,81

1,06

1,25

1,44

1,75

0,63

0,69

0,81

0,94

1,06

1,31

1,50

2,06

2,31

0,63

0,75

0,88

1,00

1,13

1,38

1,56

2,13

2,38

3,25

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| width | thickness | article code |  | width | thickness | article code |
| 5 | 2 | 27100502 |  | 12 | 2 | 27101202 |
| 5 | 3 | 27100503 |  | 12 | 3 | 27101203 |
| 5 | 4 | 27100504 |  | 12 | 4 | 27101204 |
| 5 | 5 | 27100505 |  | 12 | 5 | 27101205 |
|  |  |  |  | 12 | 6 | 27101206 |
| 6 | 2 | 27100602 |  | 12 | 8 | 27101208 |
| 6 | 3 | 27100603 |  | 12 | 10 | 27101210 |
| 6 | 4 | 27100604 |  | 12 | 12 | 27101212 |
| 6 | 5 | 27100605 |  |  |  |  |
| 6 | 6 | 27100606 |  | 15 | 2 | 27101502 |
|  |  |  |  | 15 | 3 | 27101503 |
| 7 | 2 | 27100702 |  | 15 | 4 | 27101504 |
| 7 | 3 | 27100703 |  | 15 | 5 | 27101505 |
| 7 | 4 | 27100704 |  | 15 | 6 | 27101506 |
| 7 | 5 | 27100705 |  | 15 | 8 | 27101508 |
| 7 | 6 | 27100706 |  | 15 | 10 | 27101510 |
|  |  |  |  | 15 | 12 | 27101512 |
| 8 | 2 | 27100802 |  | 15 | 15 | 27101515 |
| 8 | 3 | 27100803 |  |  |  |  |
| 8 | 4 | 27100804 |  | 18 | 2 | 27101802 |
| 8 | 5 | 27100805 |  | 18 | 3 | 27101803 |
| 8 | 6 | 27100806 |  | 18 | 4 | 27101804 |
| 8 | 8 | 27100808 |  | 18 | 5 | 27101805 |
|  |  |  |  | 18 | 6 | 27101806 |
| 9 | 2 | 27100902 |  | 18 | 8 | 27101808 |
| 9 | 3 | 27100903 |  | 18 | 10 | 27101810 |
| 9 | 4 | 27100904 |  | 18 | 12 | 27101812 |
| 9 | 5 | 27100905 |  | 18 | 15 | 27101815 |
| 9 | 6 | 27100906 |  |  |  |  |
| 9 | 8 | 27100908 |  | 20 | 2 | 27102002 |
|  |  |  |  | 20 | 3 | 27102003 |
| 10 | 2 | 27101002 |  | 20 | 4 | 27102004 |
| 10 | 3 | 27101003 |  | 20 | 5 | 27102005 |
| 10 | 4 | 27101004 |  | 20 | 6 | 27102006 |
| 10 | 5 | 27101005 |  | 20 | 8 | 27102008 |
| 10 | 6 | 27101006 |  | 20 | 10 | 27102010 |
| 10 | 8 | 27101008 |  | 20 | 12 | 27102012 |
| 10 | 10 | 27101010 |  | 20 | 15 | 27102015 |
|  |  |  |  | 20 | 20 | 27102020 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

price per m (euro)

0,81

1,00

1,13

1,25

1,44

1,69

2,19

2,31

2,75

3,88

0,88

1,13

1,31

1,44

1,63

1,88

2,38

2,69

3,19

4,38

1,06

1,31

1,50

1,69

1,88

2,19

2,69

3,25

3,69

5,06

1,19

1,44

1,63

1,94

2,13

2,50

2,94

3,81

4,13

5,69

1,38

1,63

2,19

2,50

2,81

price per m (euro)

3,25

3,94

4,81

5,50

7,19

1,75

2,25

2,63

2,88

3,25

3,75

4,75

5,38

6,38

8,75

2,06

2,56

2,94

3,38

3,75

4,38

5,31

6,50

7,31

10,00

2,19

2,63

3,31

3,75

4,25

4,94

6,13

7,13

8,25

11,06

2,38

2,88

3,50

3,88

4,25

5,00

6,25

7,63

8,19

11,38



|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| width | thickness | article code |  | width | thickness | article code |
| 25 | 2 | 27102502 |  | 50 | 8 | 27105008 |
| 25 | 3 | 27102503 |  | 50 | 10 | 27105010 |
| 25 | 4 | 27102504 |  | 50 | 12 | 27105012 |
| 25 | 5 | 27102505 |  | 50 | 15 | 27105015 |
| 25 | 6 | 27102506 |  | 50 | 20 | 27105020 |
| 25 | 8 | 27102508 |  |  |  |  |
| 25 | 10 | 27102510 |  | 60 | 2 | 27106002 |
| 25 | 12 | 27102512 |  | 60 | 3 | 27106003 |
| 25 | 15 | 27102515 |  | 60 | 4 | 27106004 |
| 25 | 20 | 27102520 |  | 60 | 5 | 27106005 |
|  |  |  |  | 60 | 6 | 27106006 |
| 30 | 2 | 27103002 |  | 60 | 8 | 27106008 |
| 30 | 3 | 27103003 |  | 60 | 10 | 27106010 |
| 30 | 4 | 27103004 |  | 60 | 12 | 27106012 |
| 30 | 5 | 27103005 |  | 60 | 15 | 27106015 |
| 30 | 6 | 27103006 |  | 60 | 20 | 27106020 |
| 30 | 8 | 27103008 |  |  |  |  |
| 30 | 10 | 27103010 |  | 70 | 2 | 27107002 |
| 30 | 12 | 27103012 |  | 70 | 3 | 27107003 |
| 30 | 15 | 27103015 |  | 70 | 4 | 27107004 |
| 30 | 20 | 27103020 |  | 70 | 5 | 27107005 |
|  |  |  |  | 70 | 6 | 27107006 |
| 35 | 2 | 27103502 |  | 70 | 8 | 27107008 |
| 35 | 3 | 27103503 |  | 70 | 10 | 27107010 |
| 35 | 4 | 27103504 |  | 70 | 12 | 27107012 |
| 35 | 5 | 27103505 |  | 70 | 15 | 27107015 |
| 35 | 6 | 27103506 |  | 70 | 20 | 27107020 |
| 35 | 8 | 27103508 |  |  |  |  |
| 35 | 10 | 27103510 |  | 75 | 2 | 27107502 |
| 35 | 12 | 27103512 |  | 75 | 3 | 27107503 |
| 35 | 15 | 27103515 |  | 75 | 4 | 27107504 |
| 35 | 20 | 27103520 |  | 75 | 5 | 27107505 |
|  |  |  |  | 75 | 6 | 27107506 |
| 40 | 2 | 27104002 |  | 75 | 8 | 27107508 |
| 40 | 3 | 27104003 |  | 75 | 10 | 27107510 |
| 40 | 4 | 27104004 |  | 75 | 12 | 27107512 |
| 40 | 5 | 27104005 |  | 75 | 15 | 27107515 |
| 40 | 6 | 27104006 |  | 75 | 20 | 27107520 |
| 40 | 8 | 27104008 |  |  |  |  |
| 40 | 10 | 27104010 |  | 80 | 2 | 27108002 |
| 40 | 12 | 27104012 |  | 80 | 3 | 27108003 |
| 40 | 15 | 27104015 |  | 80 | 4 | 27108004 |
| 40 | 20 | 27104020 |  | 80 | 5 | 27108005 |
|  |  |  |  | 80 | 6 | 27108006 |
| 50 | 2 | 27105002 |  | 80 | 8 | 27108008 |
| 50 | 3 | 27105003 |  | 80 | 10 | 27108010 |
| 50 | 4 | 27105004 |  | 80 | 12 | 27108012 |
| 50 | 5 | 27105005 |  | 80 | 15 | 27108015 |
| 50 | 6 | 27105006 |  | 80 | 20 | 27108020 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

Self-adhesive CR cellular rubber strips

colour : black

cellular structure : closed

execution : one side self-adhesive layer

temperature range : -40°C to +120°C

density : 150 Kg/m3 (+/- 25)

hardness Shore 00 : 50 (+/- 5)

hardness Shore A : ca. 10 - 15 roll length (thickness 2-12 mm) : 20 meters roll length (thickness 15-20 mm) : 10 meters

price per m (euro)

2,56

3,06

3,81

4,38

4,88

5,75

6,88

8,56

9,63

12,88

2,75

3,25

4,38

5,00

5,63

6,50

7,88

9,63

11,00

14,38

4,13

4,88

6,56

7,50

8,44

9,75

11,81

14,44

16,50

21,56

price per m (euro)

5,50

6,50

8,75

10,00

11,25

13,00

15,75

19,25

22,00

28,75

6,88

8,13

10,94

12,50

14,06

16,25

19,69

24,06

27,50

35,94

8,25

9,75

13,13

15,00

16,88

19,50

23,63

28,88

33,00

43,13

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| width | thickness | article code |  | width | thickness | article code |
| 90 | 2 | 27109002 |  | 200 | 2 | 27120002 |
| 90 | 3 | 27109003 |  | 200 | 3 | 27120003 |
| 90 | 4 | 27109004 |  | 200 | 4 | 27120004 |
| 90 | 5 | 27109005 |  | 200 | 5 | 27120005 |
| 90 | 6 | 27109006 |  | 200 | 6 | 27120006 |
| 90 | 8 | 27109008 |  | 200 | 8 | 27120008 |
| 90 | 10 | 27109010 |  | 200 | 10 | 27120010 |
| 90 | 12 | 27109012 |  | 200 | 12 | 27120012 |
| 90 | 15 | 27109015 |  | 200 | 15 | 27120015 |
| 90 | 20 | 27109020 |  | 200 | 20 | 27120020 |
|  |  |  |  |  |  |  |
| 100 | 2 | 27110002 |  | 250 | 2 | 27125002 |
| 100 | 3 | 27110003 |  | 250 | 3 | 27125003 |
| 100 | 4 | 27110004 |  | 250 | 4 | 27125004 |
| 100 | 5 | 27110005 |  | 250 | 5 | 27125005 |
| 100 | 6 | 27110006 |  | 250 | 6 | 27125006 |
| 100 | 8 | 27110008 |  | 250 | 8 | 27125008 |
| 100 | 10 | 27110010 |  | 250 | 10 | 27125010 |
| 100 | 12 | 27110012 |  | 250 | 12 | 27125012 |
| 100 | 15 | 27110015 |  | 250 | 15 | 27125015 |
| 100 | 20 | 27110020 |  | 250 | 20 | 27125020 |
|  |  |  |  |  |  |  |
| 150 | 2 | 27115002 |  | 300 | 2 | 27130002 |
| 150 | 3 | 27115003 |  | 300 | 3 | 27130003 |
| 150 | 4 | 27115004 |  | 300 | 4 | 27130004 |
| 150 | 5 | 27115005 |  | 300 | 5 | 27130005 |
| 150 | 6 | 27115006 |  | 300 | 6 | 27130006 |
| 150 | 8 | 27115008 |  | 300 | 8 | 27130008 |
| 150 | 10 | 27115010 |  | 300 | 10 | 27130010 |
| 150 | 12 | 27115012 |  | 300 | 12 | 27130012 |
| 150 | 15 | 27115015 |  | 300 | 15 | 27130015 |
| 150 | 20 | 27115020 |  | 300 | 20 | 27130020 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

ces are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

Pri

price per m (euro)

11,00

13,00

17,50

20,00

22,50

26,00

31,50

38,50

44,00

57,50

12,10

14,30

19,25

22,00

24,75

28,60

34,65

42,35

48,40

63,25

13,86

16,38

22,05

25,20

28,35

32,76

39,69

48,51

55,44

72,45

price per m (euro)

15,40

18,20

24,50

28,00

31,50

36,40

44,10

53,90

61,60

80,50

16,50

19,50

26,25

30,00

33,75

39,00

47,25

57,75

66,00

86,25



|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| width | thickness | article code |  | width | thickness | article code |
| 400 | 2 | 27140002 |  | 700 | 2 | 27170002 |
| 400 | 3 | 27140003 |  | 700 | 3 | 27170003 |
| 400 | 4 | 27140004 |  | 700 | 4 | 27170004 |
| 400 | 5 | 27140005 |  | 700 | 5 | 27170005 |
| 400 | 6 | 27140006 |  | 700 | 6 | 27170006 |
| 400 | 8 | 27140008 |  | 700 | 8 | 27170008 |
| 400 | 10 | 27140010 |  | 700 | 10 | 27170010 |
| 400 | 12 | 27140012 |  | 700 | 12 | 27170012 |
| 400 | 15 | 27140015 |  | 700 | 15 | 27170015 |
| 400 | 20 | 27140020 |  | 700 | 20 | 27170020 |
|  |  |  |  |  |  |  |
| 500 | 2 | 27150002 |  | 750 | 2 | 27175002 |
| 500 | 3 | 27150003 |  | 750 | 3 | 27175003 |
| 500 | 4 | 27150004 |  | 750 | 4 | 27175004 |
| 500 | 5 | 27150005 |  | 750 | 5 | 27175005 |
| 500 | 6 | 27150006 |  | 750 | 6 | 27175006 |
| 500 | 8 | 27150008 |  | 750 | 8 | 27175008 |
| 500 | 10 | 27150010 |  | 750 | 10 | 27175010 |
| 500 | 12 | 27150012 |  | 750 | 12 | 27175012 |
| 500 | 15 | 27150015 |  | 750 | 15 | 27175015 |
| 500 | 20 | 27150020 |  | 750 | 20 | 27175020 |
|  |  |  |  |  |  |  |
| 600 | 2 | 27160002 |  |  |  |  |
| 600 | 3 | 27160003 |  |  |  |  |
| 600 | 4 | 27160004 |  |  |  |  |
| 600 | 5 | 27160005 |  |  |  |  |
| 600 | 6 | 27160006 |  |  |  |  |
| 600 | 8 | 27160008 |  |  |  |  |
| 600 | 10 | 27160010 |  |  |  |  |
| 600 | 12 | 27160012 |  |  |  |  |
| 600 | 15 | 27160015 |  |  |  |  |
| 600 | 20 | 27160020 |  |  |  |  |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

Self-adhesive NBR cellular rubber sheeting

quality : NBR/PVC

colour : black

cellular structure : closed

execution : one side self-adhesive layer

temperature range : -40°C to +100°C

density : 195 Kg/m3 (+/- 25)

hardness Shore 00 : 55 (+/- 5)

hardness Shore A : ca. 10 - 15

price per m2 (euro)

19,50

24,00

31,00

34,00

39,00

45,00

54,00

|  |  |  |  |
| --- | --- | --- | --- |
| article code | thickness (mm) | width (mm) | length (mm) |

|  |  |  |  |
| --- | --- | --- | --- |
| 27900002 | 2 | 1000 | 10000 |
| 27900003 | 3 | 1000 | 10000 |
| 27900004 | 4 | 1000 | 10000 |
| 27900005 | 5 | 1000 | 10000 |
| 27900006 | 6 | 1000 | 10000 |
| 27900008 | 8 | 1000 | 10000 |
| 27900010 | 10 | 1000 | 10000 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

Self-adhesive NBR/PVC cellular rubber strips

quality : NBR/PVC

colour : black

cellular structure : closed

execution : one side self-adhesive layer

temperature range : -40°C to +100°C

density : 195 Kg/m3 (+/- 25)

hardness Shore 00 : 55 (+/- 5)

hardness Shore A : ca. 10 - 15 roll length (thickness 2-10 mm) : 10 meters

price per m (euro)

0,48

0,50

0,57

0,64

0,48

0,50

0,57

0,57

0,72

0,49

0,50

0,57

0,64

0,72

0,49

0,50

0,57

0,64

0,72

0,79

0,51

0,57

0,59

0,72

0,79

1,00

0,51

0,57

0,61

0,72

0,82

0,98

1,17

price per m (euro)

0,57

0,65

0,72

0,78

0,91

1,07

1,22

0,65

0,72

0,78

0,86

0,98

1,17

1,43

0,72

0,79

0,93

1,07

1,22

1,50

1,72

0,72

0,85

1,04

1,17

1,30

1,56

1,76

0,91

1,11

1,30

1,43

1,69

1,95

2,47

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| width | thickness | article code |  | width | thickness | article code |
| 5 | 2 | 27400502 |  | 12 | 2 | 27401202 |
| 5 | 3 | 27400503 |  | 12 | 3 | 27401203 |
| 5 | 4 | 27400504 |  | 12 | 4 | 27401204 |
| 5 | 5 | 27400505 |  | 12 | 5 | 27401205 |
|  |  |  |  | 12 | 6 | 27401206 |
| 6 | 2 | 27400602 |  | 12 | 8 | 27401208 |
| 6 | 3 | 27400603 |  | 12 | 10 | 27401210 |
| 6 | 4 | 27400604 |  |  |  |  |
| 6 | 5 | 27400605 |  | 15 | 2 | 27401502 |
| 6 | 6 | 27400606 |  | 15 | 3 | 27401503 |
|  |  |  |  | 15 | 4 | 27401504 |
| 7 | 2 | 27400702 |  | 15 | 5 | 27401505 |
| 7 | 3 | 27400703 |  | 15 | 6 | 27401506 |
| 7 | 4 | 27400704 |  | 15 | 8 | 27401508 |
| 7 | 5 | 27400705 |  | 15 | 10 | 27401510 |
| 7 | 6 | 27400706 |  |  |  |  |
|  |  |  |  | 18 | 2 | 27401802 |
| 8 | 2 | 27400802 |  | 18 | 3 | 27401803 |
| 8 | 3 | 27400803 |  | 18 | 4 | 27401804 |
| 8 | 4 | 27400804 |  | 18 | 5 | 27401805 |
| 8 | 5 | 27400805 |  | 18 | 6 | 27401806 |
| 8 | 6 | 27400806 |  | 18 | 8 | 27401808 |
| 8 | 8 | 27400808 |  | 18 | 10 | 27401810 |
|  |  |  |  |  |  |  |
| 9 | 2 | 27400902 |  | 20 | 2 | 27402002 |
| 9 | 3 | 27400903 |  | 20 | 3 | 27402003 |
| 9 | 4 | 27400904 |  | 20 | 4 | 27402004 |
| 9 | 5 | 27400905 |  | 20 | 5 | 27402005 |
| 9 | 6 | 27400906 |  | 20 | 6 | 27402006 |
| 9 | 8 | 27400908 |  | 20 | 8 | 27402008 |
|  |  |  |  | 20 | 10 | 27402010 |
| 10 | 2 | 27401002 |  |  |  |  |
| 10 | 3 | 27401003 |  | 25 | 2 | 27402502 |
| 10 | 4 | 27401004 |  | 25 | 3 | 27402503 |
| 10 | 5 | 27401005 |  | 25 | 4 | 27402504 |
| 10 | 6 | 27401006 |  | 25 | 5 | 27402505 |
| 10 | 8 | 27401008 |  | 25 | 6 | 27402506 |
| 10 | 10 | 27401010 |  | 25 | 8 | 27402508 |
|  |  |  |  | 25 | 10 | 27402510 |

Self-adhesive NBR/PVC cellular rubber strips

quality : NBR/PVC

colour : black

cellular structure : closed

execution : one side self-adhesive layer

temperature range : -40°C to +100°C

density : 195 Kg/m3 (+/- 25)

hardness Shore 00 : 55 (+/- 5)

hardness Shore A : ca. 10 - 15 roll length (thickness 2-10 mm) : 10 meters

price per m (euro)

0,98

1,30

1,56

1,69

1,89

2,08

2,73

1,17

1,43

1,69

1,95

2,15

2,47

3,12

1,37

1,69

1,89

2,21

2,47

2,86

3,38

1,56

1,95

2,60

2,86

3,25

3,77

4,55

1,95

2,34

2,99

3,51

3,64

4,29

5,46

price per m (euro)

2,36

2,67

3,36

3,90

4,29

5,01

6,08

2,50

3,00

3,79

4,29

4,86

5,65

7,01

2,72

3,25

4,01

4,42

4,94

5,72

7,35

2,86

3,50

4,29

4,94

5,46

6,50

7,80

3,12

3,77

5,20

5,72

6,50

7,28

8,97

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| width | thickness | article code |  | width | thickness | article code |
| 30 | 2 | 27403002 |  | 70 | 2 | 27407002 |
| 30 | 3 | 27403003 |  | 70 | 3 | 27407003 |
| 30 | 4 | 27403004 |  | 70 | 4 | 27407004 |
| 30 | 5 | 27403005 |  | 70 | 5 | 27407005 |
| 30 | 6 | 27403006 |  | 70 | 6 | 27407006 |
| 30 | 8 | 27403008 |  | 70 | 8 | 27407008 |
| 30 | 10 | 27403010 |  | 70 | 10 | 27407010 |
|  |  |  |  |  |  |  |
| 35 | 2 | 27403502 |  | 75 | 2 | 27407502 |
| 35 | 3 | 27403503 |  | 75 | 3 | 27407503 |
| 35 | 4 | 27403504 |  | 75 | 4 | 27407504 |
| 35 | 5 | 27403505 |  | 75 | 5 | 27407505 |
| 35 | 6 | 27403506 |  | 75 | 6 | 27407506 |
| 35 | 8 | 27403508 |  | 75 | 8 | 27407508 |
| 35 | 10 | 27403510 |  | 75 | 10 | 27407510 |
|  |  |  |  |  |  |  |
| 40 | 2 | 27404002 |  | 80 | 2 | 27408002 |
| 40 | 3 | 27404003 |  | 80 | 3 | 27408003 |
| 40 | 4 | 27404004 |  | 80 | 4 | 27408004 |
| 40 | 5 | 27404005 |  | 80 | 5 | 27408005 |
| 40 | 6 | 27404006 |  | 80 | 6 | 27408006 |
| 40 | 8 | 27404008 |  | 80 | 8 | 27408008 |
| 40 | 10 | 27404010 |  | 80 | 10 | 27408010 |
|  |  |  |  |  |  |  |
| 50 | 2 | 27405002 |  | 90 | 2 | 27409002 |
| 50 | 3 | 27405003 |  | 90 | 3 | 27409003 |
| 50 | 4 | 27405004 |  | 90 | 4 | 27409004 |
| 50 | 5 | 27405005 |  | 90 | 5 | 27409005 |
| 50 | 6 | 27405006 |  | 90 | 6 | 27409006 |
| 50 | 8 | 27405008 |  | 90 | 8 | 27409008 |
| 50 | 10 | 27405010 |  | 90 | 10 | 27409010 |
|  |  |  |  |  |  |  |
| 60 | 2 | 27406002 |  | 100 | 2 | 27410002 |
| 60 | 3 | 27406003 |  | 100 | 3 | 27410003 |
| 60 | 4 | 27406004 |  | 100 | 4 | 27410004 |
| 60 | 5 | 27406005 |  | 100 | 5 | 27410005 |
| 60 | 6 | 27406006 |  | 100 | 6 | 27410006 |
| 60 | 8 | 27406008 |  | 100 | 8 | 27410008 |
| 60 | 10 | 27406010 |  | 100 | 10 | 27410010 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

price per m (euro)

4,72

5,58

7,51

8,58

9,65

11,15

13,51

6,29

7,44

10,01

11,44

12,87

14,87

18,02

7,87

9,30

12,51

14,30

16,09

18,59

22,52

9,09

10,75

14,47

16,54

18,60

21,50

26,04

12,13

14,33

19,29

22,05

24,80

28,66

34,73

price per m (euro)

14,30

16,90

22,75

26,00

29,25

33,80

40,95

15,44

18,25

24,57

28,08

31,59

36,50

44,23

16,82

19,87

26,75

30,58

34,40

39,75

48,16

17,59

20,79

27,98

31,98

35,98

41,57

50,37



|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| width | thickness | article code |  | width | thickness | article code |
| 150 | 2 | 27415002 |  | 500 | 2 | 27450002 |
| 150 | 3 | 27415003 |  | 500 | 3 | 27450003 |
| 150 | 4 | 27415004 |  | 500 | 4 | 27450004 |
| 150 | 5 | 27415005 |  | 500 | 5 | 27450005 |
| 150 | 6 | 27415006 |  | 500 | 6 | 27450006 |
| 150 | 8 | 27415008 |  | 500 | 8 | 27450008 |
| 150 | 10 | 27415010 |  | 500 | 10 | 27450010 |
|  |  |  |  |  |  |  |
| 200 | 2 | 27420002 |  | 600 | 2 | 27460002 |
| 200 | 3 | 27420003 |  | 600 | 3 | 27460003 |
| 200 | 4 | 27420004 |  | 600 | 4 | 27460004 |
| 200 | 5 | 27420005 |  | 600 | 5 | 27460005 |
| 200 | 6 | 27420006 |  | 600 | 6 | 27460006 |
| 200 | 8 | 27420008 |  | 600 | 8 | 27460008 |
| 200 | 10 | 27420010 |  | 600 | 10 | 27460010 |
|  |  |  |  |  |  |  |
| 250 | 2 | 27425002 |  | 700 | 2 | 27470002 |
| 250 | 3 | 27425003 |  | 700 | 3 | 27470003 |
| 250 | 4 | 27425004 |  | 700 | 4 | 27470004 |
| 250 | 5 | 27425005 |  | 700 | 5 | 27470005 |
| 250 | 6 | 27425006 |  | 700 | 6 | 27470006 |
| 250 | 8 | 27425008 |  | 700 | 8 | 27470008 |
| 250 | 10 | 27425010 |  | 700 | 10 | 27470010 |
|  |  |  |  |  |  |  |
| 300 | 2 | 27430002 |  | 750 | 2 | 27475002 |
| 300 | 3 | 27430003 |  | 750 | 3 | 27475003 |
| 300 | 4 | 27430004 |  | 750 | 4 | 27475004 |
| 300 | 5 | 27430005 |  | 750 | 5 | 27475005 |
| 300 | 6 | 27430006 |  | 750 | 6 | 27475006 |
| 300 | 8 | 27430008 |  | 750 | 8 | 27475008 |
| 300 | 10 | 27430010 |  | 750 | 10 | 27475010 |
|  |  |  |  |  |  |  |
| 400 | 2 | 27440002 |  |  |  |  |
| 400 | 3 | 27440003 |  |  |  |  |
| 400 | 4 | 27440004 |  |  |  |  |
| 400 | 5 | 27440005 |  |  |  |  |
| 400 | 6 | 27440006 |  |  |  |  |
| 400 | 8 | 27440008 |  |  |  |  |
| 400 | 10 | 27440010 |  |  |  |  |

Silicone foam sheeting

colour : white

cellular structure : closed execution : without adhesive temperature range : -70°C to +200°C

density : 250 Kg/m3 (+/- 40)

hardness Shore 00 : 55 (+/- 5) hardness Shore A : ca. 10

price per m2 (euro)

134,75

151,25

167,20

176,00

181,50

231,00

247,50

286,00

374,00

467,50

605,00

|  |  |  |  |
| --- | --- | --- | --- |
| article code | thickness (mm) | width (mm) | length (mm) |

|  |  |  |  |
| --- | --- | --- | --- |
| 29100002 | 2 | 1000 | 10000 |
| 29100003 | 3 | 1000 | 10000 |
| 29100004 | 4 | 1000 | 10000 |
| 29100005 | 5 | 1000 | 10000 |
| 29100006 | 6 | 1000 | 10000 |
| 29100008 | 8 | 1000 | 10000 |
| 29100010 | 10 | 1000 | 10000 |
| 29100012 | 12 | 1000 | 1000 |
| 29100015 | 15 | 1000 | 1000 |
| 29100020 | 20 | 1000 | 1000 |
| 29100025 | 25 | 1000 | 1000 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

Silicone foam sheeting with self-adhesive

colour : white cellular structure : closed

execution : one side self-adhesive layer temperature range : -70°C to +200°C

density : 250 Kg/m3 (+/- 40)

hardness Shore 00 : 55 (+/- 5) hardness Shore A : ca. 10

price per m2 (euro)

145,75

151,25

211,20

220,00

225,50

275,00

291,50

|  |  |  |  |
| --- | --- | --- | --- |
| article code | thickness (mm) | width (mm) | length (mm) |

|  |  |  |  |
| --- | --- | --- | --- |
| 29110002 | 2 | 1000 | 10000 |
| 29110003 | 3 | 1000 | 10000 |
| 29110004 | 4 | 1000 | 10000 |
| 29110005 | 5 | 1000 | 10000 |
| 29110006 | 6 | 1000 | 10000 |
| 29110008 | 8 | 1000 | 10000 |
| 29110010 | 10 | 1000 | 10000 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

Silicone foam strip

colour : white

cellular structure : closed execution : without adhesive temperature range : -70°C to +200°C

density : 250 Kg/m3 (+/- 40)

hardness Shore 00 : 55 (+/- 5) hardness Shore A : ca. 10

roll length : 10 meters

price per m (euro)

0,83

0,86

1,20

1,25

1,00

1,04

1,45

1,51

1,54

1,16

1,21

1,69

1,76

1,80

1,33

1,38

1,93

2,01

2,06

2,51

1,50

1,55

2,17

2,26

2,32

2,82

1,66

1,73

2,41

2,51

2,57

3,14

3,33

price per m (euro)

2,00

2,07

2,89

3,01

3,09

3,76

3,99

2,49

2,59

3,61

3,76

3,86

4,71

4,99

2,99

3,11

4,34

4,52

4,63

5,65

5,99

3,33

3,45

4,82

5,02

5,15

6,27

6,65

4,16

4,31

6,02

6,27

6,43

7,84

8,31

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| width | thickness | article code |  | width | thickness | article code |
| 5 | 2 | 29300502 |  | 12 | 2 | 29301202 |
| 5 | 3 | 29300503 |  | 12 | 3 | 29301203 |
| 5 | 4 | 29300504 |  | 12 | 4 | 29301204 |
| 5 | 5 | 29300505 |  | 12 | 5 | 29301205 |
|  |  |  |  | 12 | 6 | 29301206 |
| 6 | 2 | 29300602 |  | 12 | 8 | 29301208 |
| 6 | 3 | 29300603 |  | 12 | 10 | 29301210 |
| 6 | 4 | 29300604 |  |  |  |  |
| 6 | 5 | 29300605 |  | 15 | 2 | 29301502 |
| 6 | 6 | 29300606 |  | 15 | 3 | 29301503 |
|  |  |  |  | 15 | 4 | 29301504 |
| 7 | 2 | 29300702 |  | 15 | 5 | 29301505 |
| 7 | 3 | 29300702 |  | 15 | 6 | 29301506 |
| 7 | 4 | 29300702 |  | 15 | 8 | 29301508 |
| 7 | 5 | 29300702 |  | 15 | 10 | 29301510 |
| 7 | 6 | 29300702 |  |  |  |  |
|  |  |  |  | 18 | 2 | 29301802 |
| 8 | 2 | 29300802 |  | 18 | 3 | 29301803 |
| 8 | 3 | 29300803 |  | 18 | 4 | 29301804 |
| 8 | 4 | 29300804 |  | 18 | 5 | 29301805 |
| 8 | 5 | 29300805 |  | 18 | 6 | 29301806 |
| 8 | 6 | 29300806 |  | 18 | 8 | 29301808 |
| 8 | 8 | 29300808 |  | 18 | 10 | 29301810 |
|  |  |  |  |  |  |  |
| 9 | 2 | 29300902 |  | 20 | 2 | 29302002 |
| 9 | 3 | 29300903 |  | 20 | 3 | 29302003 |
| 9 | 4 | 29300904 |  | 20 | 4 | 29302004 |
| 9 | 5 | 29300905 |  | 20 | 5 | 29302005 |
| 9 | 6 | 29300906 |  | 20 | 6 | 29302006 |
| 9 | 8 | 29300908 |  | 20 | 8 | 29302008 |
|  |  |  |  | 20 | 10 | 29302010 |
| 10 | 2 | 29301002 |  |  |  |  |
| 10 | 3 | 29301003 |  | 25 | 2 | 29302502 |
| 10 | 4 | 29301004 |  | 25 | 3 | 29302503 |
| 10 | 5 | 29301005 |  | 25 | 4 | 29302504 |
| 10 | 6 | 29301006 |  | 25 | 5 | 29302505 |
| 10 | 8 | 29301008 |  | 25 | 6 | 29302506 |
| 10 | 10 | 29301010 |  | 25 | 8 | 29302508 |
|  |  |  |  | 25 | 10 | 29302510 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

price per m (euro)

4,99

5,18

7,23

7,53

7,72

9,41

9,98

6,32

6,56

9,16

9,54

9,78

11,92

12,64

6,65

6,90

9,64

10,04

10,29

12,55

13,30

8,31

8,63

12,05

12,55

12,86

15,69

16,63

9,98

10,35

14,46

15,06

15,44

18,82

19,95

11,64

12,08

16,87

17,57

18,01

21,96

23,28

price per m (euro)

12,47

12,94

18,07

18,82

19,30

23,53

24,94

13,30

13,80

19,28

20,08

20,58

25,10

26,61

14,97

15,53

21,69

22,59

23,15

28,24

29,93

16,63

17,26

24,10

25,10

25,73

31,37

33,26

24,94

25,88

36,14

37,65

38,59

47,06

49,88

33,26

34,51

48,19

50,20

51,45

62,75

66,51



|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| width | thickness | article code |  | width | thickness | article code |
| 30 | 2 | 29303002 |  | 75 | 2 | 29307502 |
| 30 | 3 | 29303003 |  | 75 | 3 | 29307503 |
| 30 | 4 | 29303004 |  | 75 | 4 | 29307504 |
| 30 | 5 | 29303005 |  | 75 | 5 | 29307505 |
| 30 | 6 | 29303006 |  | 75 | 6 | 29307506 |
| 30 | 8 | 29303008 |  | 75 | 8 | 29307508 |
| 30 | 10 | 29303010 |  | 75 | 10 | 29307510 |
|  |  |  |  |  |  |  |
| 38 | 2 | 29303802 |  | 80 | 2 | 29308002 |
| 38 | 3 | 29303803 |  | 80 | 3 | 29308003 |
| 38 | 4 | 29303804 |  | 80 | 4 | 29308004 |
| 38 | 5 | 29303805 |  | 80 | 5 | 29308005 |
| 38 | 6 | 29303806 |  | 80 | 6 | 29308006 |
| 38 | 8 | 29303808 |  | 80 | 8 | 29308008 |
| 38 | 10 | 29303810 |  | 80 | 10 | 29308010 |
|  |  |  |  |  |  |  |
| 40 | 2 | 29304002 |  | 90 | 2 | 29309002 |
| 40 | 3 | 29304003 |  | 90 | 3 | 29309003 |
| 40 | 4 | 29304004 |  | 90 | 4 | 29309004 |
| 40 | 5 | 29304005 |  | 90 | 5 | 29309005 |
| 40 | 6 | 29304006 |  | 90 | 6 | 29309006 |
| 40 | 8 | 29304008 |  | 90 | 8 | 29309008 |
| 40 | 10 | 29304010 |  | 90 | 10 | 29309010 |
|  |  |  |  |  |  |  |
| 50 | 2 | 29305002 |  | 100 | 2 | 29310002 |
| 50 | 3 | 29305003 |  | 100 | 3 | 29310003 |
| 50 | 4 | 29305004 |  | 100 | 4 | 29310004 |
| 50 | 5 | 29305005 |  | 100 | 5 | 29310005 |
| 50 | 6 | 29305006 |  | 100 | 6 | 29310006 |
| 50 | 8 | 29305008 |  | 100 | 8 | 29310008 |
| 50 | 10 | 29305010 |  | 100 | 10 | 29310010 |
|  |  |  |  |  |  |  |
| 60 | 2 | 29306002 |  | 150 | 2 | 29315002 |
| 60 | 3 | 29306003 |  | 150 | 3 | 29315003 |
| 60 | 4 | 29306004 |  | 150 | 4 | 29315004 |
| 60 | 5 | 29306005 |  | 150 | 5 | 29315005 |
| 60 | 6 | 29306006 |  | 150 | 6 | 29315006 |
| 60 | 8 | 29306008 |  | 150 | 8 | 29315008 |
| 60 | 10 | 29306010 |  | 150 | 10 | 29315010 |
|  |  |  |  |  |  |  |
| 70 | 2 | 29307002 |  | 200 | 2 | 29320002 |
| 70 | 3 | 29307003 |  | 200 | 3 | 29320003 |
| 70 | 4 | 29307004 |  | 200 | 4 | 29320004 |
| 70 | 5 | 29307005 |  | 200 | 5 | 29320005 |
| 70 | 6 | 29307006 |  | 200 | 6 | 29320006 |
| 70 | 8 | 29307008 |  | 200 | 8 | 29320008 |
| 70 | 10 | 29307010 |  | 200 | 10 | 29320010 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

Self-adhesive silicone foam strips

colour : white

cellular structure : closed

execution : one side self-adhesive layer temperature range : -70°C to +200°C

density : 250 Kg/m3 (+/- 40)

hardness Shore 00 : 55 (+/- 5) hardness Shore A : ca. 10

roll length : 10 meters

price per m (euro)

1,00

1,04

1,45

1,51

1,20

1,25

1,74

1,81

1,86

1,40

1,46

2,03

2,12

2,17

1,60

1,66

2,32

2,42

2,48

3,02

1,80

1,87

2,61

2,72

2,79

3,40

2,00

2,08

2,90

3,02

3,10

3,78

4,01

price per m (euro)

2,40

2,49

3,48

3,63

3,72

4,54

4,81

3,01

3,12

4,35

4,54

4,65

5,67

6,01

3,61

3,74

5,23

5,44

5,58

6,80

7,21

4,01

4,16

5,81

6,05

6,20

7,56

8,01

5,01

5,20

7,26

7,56

7,75

9,45

10,02

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| width | thickness | article code |  | width | thickness | article code |
| 5 | 2 | 29200502 |  | 12 | 2 | 29201202 |
| 5 | 3 | 29200503 |  | 12 | 3 | 29201203 |
| 5 | 4 | 29200504 |  | 12 | 4 | 29201204 |
| 5 | 5 | 29200505 |  | 12 | 5 | 29201205 |
|  |  |  |  | 12 | 6 | 29201206 |
| 6 | 2 | 29200602 |  | 12 | 8 | 29201208 |
| 6 | 3 | 29200603 |  | 12 | 10 | 29201210 |
| 6 | 4 | 29200604 |  |  |  |  |
| 6 | 5 | 29200605 |  | 15 | 2 | 29201502 |
| 6 | 6 | 29200606 |  | 15 | 3 | 29201503 |
|  |  |  |  | 15 | 4 | 29201504 |
| 7 | 2 | 29200702 |  | 15 | 5 | 29201505 |
| 7 | 3 | 29200703 |  | 15 | 6 | 29201506 |
| 7 | 4 | 29200704 |  | 15 | 8 | 29201508 |
| 7 | 5 | 29200705 |  | 15 | 10 | 29201510 |
| 7 | 6 | 29200706 |  |  |  |  |
|  |  |  |  | 18 | 2 | 29201802 |
| 8 | 2 | 29200802 |  | 18 | 3 | 29201803 |
| 8 | 3 | 29200803 |  | 18 | 4 | 29201804 |
| 8 | 4 | 29200804 |  | 18 | 5 | 29201805 |
| 8 | 5 | 29200805 |  | 18 | 6 | 29201806 |
| 8 | 6 | 29200806 |  | 18 | 8 | 29201808 |
| 8 | 8 | 29200808 |  | 18 | 10 | 29201810 |
|  |  |  |  |  |  |  |
| 9 | 2 | 29200902 |  | 20 | 2 | 29202002 |
| 9 | 3 | 29200903 |  | 20 | 3 | 29202003 |
| 9 | 4 | 29200904 |  | 20 | 4 | 29202004 |
| 9 | 5 | 29200905 |  | 20 | 5 | 29202005 |
| 9 | 6 | 29200906 |  | 20 | 6 | 29202006 |
| 9 | 8 | 29200908 |  | 20 | 8 | 29202008 |
|  |  |  |  | 20 | 10 | 29202010 |
| 10 | 2 | 29201002 |  |  |  |  |
| 10 | 3 | 29201003 |  | 25 | 2 | 29202502 |
| 10 | 4 | 29201004 |  | 25 | 3 | 29202503 |
| 10 | 5 | 29201005 |  | 25 | 4 | 29202504 |
| 10 | 6 | 29201006 |  | 25 | 5 | 29202505 |
| 10 | 8 | 29201008 |  | 25 | 6 | 29202506 |
| 10 | 10 | 29201010 |  | 25 | 8 | 29202508 |
|  |  |  |  | 25 | 10 | 29202510 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

price per m (euro)

6,01

6,24

8,71

9,07

9,30

11,34

12,02

7,61

7,90

11,03

11,49

11,78

14,36

15,23

8,01

8,32

11,61

12,10

12,40

15,12

16,03

10,02

10,40

14,52

15,12

15,50

18,90

20,03

12,02

12,47

17,42

18,14

18,60

22,68

24,04

14,02

14,55

20,32

21,17

21,70

26,46

28,05

price per m (euro)

15,03

15,59

21,77

22,68

23,25

28,35

30,05

16,03

16,63

23,22

24,19

24,80

30,24

32,05

18,03

18,71

26,13

27,22

27,90

34,02

36,06

20,03

20,79

29,03

30,24

31,00

37,80

40,07

30,05

31,19

43,55

45,36

46,49

56,70

60,10

40,07

41,58

58,06

60,48

61,99

75,60

80,14



|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| width | thickness | article code |  | width | thickness | article code |
| 30 | 2 | 29203002 |  | 75 | 2 | 29207502 |
| 30 | 3 | 29203003 |  | 75 | 3 | 29207503 |
| 30 | 4 | 29203004 |  | 75 | 4 | 29207504 |
| 30 | 5 | 29203005 |  | 75 | 5 | 29207505 |
| 30 | 6 | 29203006 |  | 75 | 6 | 29207506 |
| 30 | 8 | 29203008 |  | 75 | 8 | 29207508 |
| 30 | 10 | 29203010 |  | 75 | 10 | 29207510 |
|  |  |  |  |  |  |  |
| 38 | 2 | 29203802 |  | 80 | 2 | 29208002 |
| 38 | 3 | 29203803 |  | 80 | 3 | 29208003 |
| 38 | 4 | 29203804 |  | 80 | 4 | 29208004 |
| 38 | 5 | 29203805 |  | 80 | 5 | 29208005 |
| 38 | 6 | 29203806 |  | 80 | 6 | 29208006 |
| 38 | 8 | 29203808 |  | 80 | 8 | 29208008 |
| 38 | 10 | 29203810 |  | 80 | 10 | 29208010 |
|  |  |  |  |  |  |  |
| 40 | 2 | 29204002 |  | 90 | 2 | 29209002 |
| 40 | 3 | 29204003 |  | 90 | 3 | 29209003 |
| 40 | 4 | 29204004 |  | 90 | 4 | 29209004 |
| 40 | 5 | 29204005 |  | 90 | 5 | 29209005 |
| 40 | 6 | 29204006 |  | 90 | 6 | 29209006 |
| 40 | 8 | 29204008 |  | 90 | 8 | 29209008 |
| 40 | 10 | 29204010 |  | 90 | 10 | 29209010 |
|  |  |  |  |  |  |  |
| 50 | 2 | 29205002 |  | 100 | 2 | 29210002 |
| 50 | 3 | 29205003 |  | 100 | 3 | 29210003 |
| 50 | 4 | 29205004 |  | 100 | 4 | 29210004 |
| 50 | 5 | 29205005 |  | 100 | 5 | 29210005 |
| 50 | 6 | 29205006 |  | 100 | 6 | 29210006 |
| 50 | 8 | 29205008 |  | 100 | 8 | 29210008 |
| 50 | 10 | 29205010 |  | 100 | 10 | 29210010 |
|  |  |  |  |  |  |  |
| 60 | 2 | 29206002 |  | 150 | 2 | 29215002 |
| 60 | 3 | 29206003 |  | 150 | 3 | 29215003 |
| 60 | 4 | 29206004 |  | 150 | 4 | 29215004 |
| 60 | 5 | 29206005 |  | 150 | 5 | 29215005 |
| 60 | 6 | 29206006 |  | 150 | 6 | 29215006 |
| 60 | 8 | 29206008 |  | 150 | 8 | 29215008 |
| 60 | 10 | 29206010 |  | 150 | 10 | 29215010 |
|  |  |  |  |  |  |  |
| 70 | 2 | 29207002 |  | 200 | 2 | 29220002 |
| 70 | 3 | 29207003 |  | 200 | 3 | 29220003 |
| 70 | 4 | 29207004 |  | 200 | 4 | 29220004 |
| 70 | 5 | 29207005 |  | 200 | 5 | 29220005 |
| 70 | 6 | 29207006 |  | 200 | 6 | 29220006 |
| 70 | 8 | 29207008 |  | 200 | 8 | 29220008 |
| 70 | 10 | 29207010 |  | 200 | 10 | 29220010 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.


#### Polyether foam sheeting

The polyether foam sheeting from are primarily made of PU and are hence also called polyurethane foam sheeting. Polyether is light weight, synthetic, antiallergenic, mildew resistant, insulating and vibration damping. It has sound absorption properties and low water vapor transmission.

#### Applications:

Furniture upholstery, mattresses, thermal insulation, packaging applications and soundproofing.

Polyether foam sheeting SG 25

quality : polyether foam sheeting

colour : grey

cellular structure : open

material : polyurethane

temperature range : -10°C to +70°C

density : 25 Kg/m3

price per unit (euro)

15,00

30,00

45,00

60,00

75,00

150,00

|  |  |  |  |
| --- | --- | --- | --- |
| article code | thickness (mm) | width (mm) | length (mm) |

|  |  |  |  |
| --- | --- | --- | --- |
| 70002501 | 10 | 1200 | 2100 |
| 70002502 | 20 | 1200 | 2100 |
| 70002503 | 30 | 1200 | 2100 |
| 70002504 | 40 | 1200 | 2100 |
| 70002505 | 50 | 1200 | 2100 |
| 70002510 | 100 | 1200 | 2100 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

Polyether foam sheeting SG 35

quality : polyether foam sheeting

colour : blue

cellular structure : open

material : polyurethane

temperature range : -10°C to +70°C

density : 35 Kg/m3

price per unit (euro)

16,00

32,00

48,00

64,00

80,00

160,00

|  |  |  |  |
| --- | --- | --- | --- |
| article code | thickness (mm) | width (mm) | length (mm) |

|  |  |  |  |
| --- | --- | --- | --- |
| 70003501 | 10 | 1200 | 2100 |
| 70003502 | 20 | 1200 | 2100 |
| 70003503 | 30 | 1200 | 2100 |
| 70003504 | 40 | 1200 | 2100 |
| 70003505 | 50 | 1200 | 2100 |
| 70003510 | 100 | 1200 | 2100 |

Delivery 1-2 business days when in stock. Special sizes and colours on request

Prices are subject to change. Delivery will be solely in accordance with the general conditions of VR Trade BV.

Polyether foam sheeting, pyramid profiled SG25

quality : Polyether foam sheeting, one side pyramid profiled

colour : grey

cellular structure : open

material : polyurethane

temperature range : -10°C to +70°C

density : 25 Kg/m3

applications : Where high performance sound absorber is needed e.g. recording studios, conference rooms, garages, industrial applications.

price per unit (euro)

48,00

82,00

|  |  |  |
| --- | --- | --- |
| article code | thickness (mm) | measurements (mm) |

|  |  |  |
| --- | --- | --- |
| 69002504 | 40 | 2000 x 1000 |
| 69002507 | 70 | 2000 x 1000 |

Polyether foam sheeting, pyramid profiled SG25 self-adhesive

quality : Polyether foam sheeting, one side pyramid profiled

colour : grey

cellular structure : open

execution : one side self-adhesive layer

material : polyurethane

temperature range : -10°C to +70°C

density : 25 Kg/m3

applications : Where high performance sound absorber is needed e.g. recording studios, conference rooms, garages, industrial applications.

price per unit (euro)

32,00

42,00

|  |  |  |
| --- | --- | --- |
| article code | thickness (mm) | measurements (mm) |

|  |  |  |
| --- | --- | --- |
| 69002505 | 40 | 1000 x 500 |
| 69002508 | 70 | 1000 x 500 |

# Technical data sheet


### EPDM cellular rubber black

EPDM cellular rubber has closed cell structure, and is available as sheeting and strips or cut out products.

|  |  |  |
| --- | --- | --- |
| material properties | data | standard |

|  |  |  |
| --- | --- | --- |
| cellular structure | closed |  |
| curing agent | peroxide |  |
| colour | black |  |
| temperature range | -40°C / +95°C |  |
| temperature intermittent | +130°C |  |
| density | 120 Kg/m3 (+/- 20) |  |
| hardness Shore 00 | 40 - 55 | ASTM D 2240 |
| hardness Shore A (\*\*) | ca. 10 - 15 |  |
| thermal conductivity | 0,0501 Wm-1K-1 | ASTM C 518-04 |
| elongation | min. 150% | ASTM D 412 |
| tensile strength | 4,5 kg/cm2 (450 kPa) | ASTM D 412 |
| tear resistance | 2,8 kg/cm (0,28 kN/m) | ASTM D 624 |
| compression strength (at 25%) | 0,35 kg/cm2 (35 kPa) | ASTM 1056/2000 |
| compression strength (at 50%) | 0,7 kg/cm2 (70 kPa) | ASTM 1056/2000 |
| compression set 25% @ 22 hours | 40% | ASTM D 395 |
| compression set (30 mm) 25% @ 22 hours | 20% |  |
| fire classification | O.K. | FMVSS 302 - FIAT 50433 |
| water absorption (3 min) | 0,13% | ASTM D 1056 |
| hydrochloric acid test (0,02%) 15 min @ 90 °C | max. shrinkage 3% | EN ISO 11195-2/05 |

Additional information:

For oil and grease resistant materials, please see our CR (neoprene) or NBR materials.

(\*) The hardness of the cellular rubber materials is measured according to the Shore 00 standard. (\*\*) The mentioned data according to the Shore A specifications is only mentioned as a guide.



### EPDM cellular grey

EPDM cellular rubber has closed cell structure, and is available as sheeting and strips or cut out products.

|  |  |  |
| --- | --- | --- |
| material properties | data | standard |

|  |  |  |
| --- | --- | --- |
| material specification | RE 42/2A2 | ASTM D 1056 |
| cellular structure | closed |  |
| curing agent | peroxide |  |
| colour | grey (RAL 7033) |  |
| temperature range | -40°C / +95°C |  |
| temperature intermittent | +130°C |  |
| density | 120 Kg/m3 (+/- 10) |  |
| hardness Shore 00 (\*) | 40 (+/- 5) | ASTM D 2240 |
| hardness Shore A (\*\*) | ca. 10 - 15 |  |
| thermal conductivity | 0,0501 Wm-1K-1 | ASTM C 518-04 |
| linear shrinkage after 22 hours @ 70°C | max. 5% |  |
| elongation | min. 150% | ASTM D 412 |
| tensile strength | 4,5 kg/cm2 (450 kPa) | ASTM D 412 |
| tear resistance | 2,8 kg/cm (0,28 kN/m) | ASTM D 624 |
| compression strength (at 25%) | 0,35 kg/cm2 (35 kPa) | ASTM 1056/85 |
| compression strength (at 50%) | 0,7 kg/cm2 (70 kPa) | ASTM 1056/85 |
| compression set 25% @ 22 hours | 40% | ASTM D 395 |
| compression set (30 mm) 25% @ 22 hours | 20% |  |
| water absorption | 2% | ASTM D 1056 |

Additional information:

(\*) The hardness of the cellular rubber materials is measured according to the Shore 00 standard. (\*\*) The mentioned data according to the Shore A specifications is only mentioned as a guide.


### EPDM cellular rubber white

The EPDM cellular rubber from has a closed-cell structure and is available in sheeting, strips or cut out products.

|  |  |  |
| --- | --- | --- |
| material properties | data | standard |

|  |  |  |
| --- | --- | --- |
| material specification | RE 42/2A2 | ASTM D 1056 |
| cellular structure | closed |  |
| curing agent | peroxide |  |
| colour | white / beige |  |
| temperature range | -40°C / +95°C |  |
| temperature intermittent | +130°C |  |
| density | 120 Kg/m3 (+/- 10) |  |
| hardness Shore 00 (\*) | 40 (+/- 5) | ASTM D 2240 |
| hardness Shore A (\*\*) | ca. 10 - 15 |  |
| thermal conductivity | 0,0501 Wm-1K-1 | ASTM C 518-04 |
| linear shrinkage after 22 hours @ 70 °C | max. 5% |  |
| elongation | min. 150% | ASTM D 412 |
| tensile strength | 4,5 kg/cm2 (450 kPa) | ASTM D 412 |
| tear resistance | 2,8 kg/cm (0,28 kN/m) | ASTM D 624 |
| compression strength (at 25%) | 0,35 kg/cm2 (35 kPa) | ASTM 1056/85 |
| compression strength (at 50%) | 0,7 kg/cm2 (70 kPa) | ASTM 1056/85 |
| compression set 25% @ 22 hours | 40% | ASTM D 395 |
| compression set (30 mm) 25% @ 22 hours | 20% |  |
| fire classification | O.K. | FMVSS 302 - FIAT 50433 |
| water absorption | 2% | ASTM D 1056 |

Additional information:

(\*) The hardness of the cellular rubber materials is measured according to the Shore 00 standard. (\*\*) The mentioned data according to the Shore A specifications is only mentioned as a guide.



### EPDM cellular rubber K-profile, self-adhesive

The extruded EPDM K-profile has a closed-cell structure and is equipped with a glass fibre self-adhesive layer.

|  |  |  |
| --- | --- | --- |
| material properties | data | standard |

cellular structure closed

curing agent peroxide

colour black

temperature range -50°C / +90°C

temperature intermittent +100°C

density 350 Kg/m3 (+/- 50) ISO 2781A

hardness shore 00 (\*) ca. 45

hardness shore A (\*\*) ca. 10

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| thickness (mm) | width (mm) | cross section | colour | type | roll length (m) | compression 25% | compression 40% |

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| 2 | 8 | black | 4-top | 225 | 219 | 240 |
| 4 | 9 | black | 3-top | 125 | 273 | 533 |
| 5 | 10 | black | 4-top | 100 | 321 | 636 |
| 6 | 10 | black | 3-top(H) | 75 | 230 | 434 |
| 3 | 15 | black | 4-top | 100 | 177 | 368 |
| 8 | 15 | black | 4-top | 50 | 735 | 1400 |
| 4 | 20 | black | 4-top | 50 | 273 | 533 |

Additional information:

Tolerances according to ISO 7715 Part 3 class E2

(\*) Hardness of cellular rubber is measured according to the Shore 00 Specification

(\*\*) The mentioned data according to the Shore A specification is only mentioned as a guide.


### EPDM cellular rubber D-profile, self-adhesive

The extruded EPDM D-profile has a closed-cell structure and is equipped with a glass fibre self-adhesive layer

|  |  |  |
| --- | --- | --- |
| material properties | data | standard |

cellular structure closed

curing agent peroxide

colour black

temperature range -50°C / +90°C

temperature intermittent +100°C

density 350 Kg/m3 (+/- 50) ISO 2781A

hardness shore 00 (\*) ca. 45

hardness shore A (\*\*) ca. 10

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| thickness (mm) | width (mm) | cross section | colour | type | roll length (mm) | compression 25% | compression 40% |

6 8 black D 100 69 119

10 12 black D 2 X 35 130 175

18 10 black D 25 150 205

20 20 black D 25 200 265

Additional information:

Tolerances according to ISO 7715 Part 3 class E2

(\*) Hardness of cellular rubber is measured according to the Shore 00 Specification

(\*\*) The mentioned data according to the Shore A specification is only mentioned as a guide.




### EPDM cellular rubber P-profile, self-adhesive

The extruded EPDM D-profile has a closed-cell structure and is equipped with a glass fibre self-adhesive layer.

|  |  |  |
| --- | --- | --- |
| material properties | data | standard |

cellular structure closed

curing agent peroxide

colour black, white and brown

temperature range -50°C / +90°C

temperature intermittent +100°C

density 350 Kg/m3 (-100 / +50) ISO 2781A

hardness shore 00 (\*) ca. 45

hardness shore A (\*\*) ca. 10

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| thickness (mm) | width (mm) | cross section | colour | type | roll length (mm) | compression 25% | compression 40% |

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| 5,5 | 9 | black | P | 2 x 50 | 62 | 122 |
| 5,5 | 9 | white | P | 2 x 50 | 62 | 122 |
| 5,5 | 9 | brown | P | 2 x 50 | 62 | 122 |

Additional information:

Tolerances according to ISO 7715 Part 3 class E2

(\*) Hardness of cellular rubber is measured according to the Shore 00 Specification

(\*\*) The mentioned data according to the Shore A specification is only mentioned as a guide.


### CR (Neoprene) cellular rubber

The CR (Neoprene) cellular rubber has a closed-cell structure and is available in sheeting, strips or cut out products.

|  |  |  |
| --- | --- | --- |
| material properties | data | standard |

|  |  |  |
| --- | --- | --- |
| material specification | SCE 42-2C2 / SBE 42-2B2 | ASTM D 1056 |
| cellular structure | closed |  |
| curing agent | peroxide |  |
| colour | black |  |
| temperature range | -40°C / +120°C | ASTM D 1056 |
| density | 150 Kg/m3 (+/- 25) | ISO 845-88 / ASTM D 3575 |
| hardness Shore 00 (\*) | 50 (+/- 5) | ASTM D 2240 |
| hardness Shore A (\*\*) | ca. 10 - 15 |  |
| thermal conductivity | 0,0384 Wm-1K-1 | ASTM C 518-04 |
| linear shrinkage after 168 hours @ 70 °C | max. 4% | ASTM D 1204 |
| elongation | min. 250% | ASTM D 412 |
| tensile strength | 11,50 kg/cm2 (1150 kPa) | ASTM D 412 |
| tear resistance | 4,3 kg/cm (0,43 kN/m) | ASTM D 624 |
| compression strength (at 25%) | 0,40 kg/cm2 (40 kPa) | ASTM 1056/85 |
| compression set 50% @ 22 hours | 25% | ASTM D 395 |
| water absorption | 2% | ASTM D 1056 |
| immersion in oil IRM 903 (22 hours at 70°C) | -18.5% | ASTM D 471/98 |
| extract test in solvents (cyclohexane acetone) | 32.7% | VDA 675 125/92 |
| aging resistant (air+UV) | good |  |
| fire test (30 mm material) | O.K. | EN ISO 11195-2/05 |
| fire classification | O.K. : HF1 | UL 94 - HF1 van 2 t/m 8 mm |
| fire classification | O.K. : V0 | UL 94 - VO van 10 t/m 40 mm |

Additional information:

(\*) The hardness of the cellular rubber materials is measured according to the Shore 00 standard. (\*\*) The mentioned data according to the Shore A specifications is only mentioned as a guide.


### NBR (Nitrile) cellular rubber

The NBR/PVC cellular rubber has a closed-cell structure and is available in sheeting, strips or cut out products.

|  |  |  |
| --- | --- | --- |
| material properties | data | standard |

|  |  |  |
| --- | --- | --- |
| material specification | SBE 42-43 / 2B2-2B3 | ASTM D 1056 |
| cellular structure | closed |  |
| curing agent | peroxide |  |
| colour | black |  |
| temperature range | -40°C / +100°C | ASTM D 1056 |
| density | 195 Kg/m3 (+/- 25) | ISO 845-88 / ASTM D 3575 |
| hardness Shore 00 (\*) | 55 (+/- 5) | ASTM D 2240 |
| hardness Shore A (\*\*) | ca. 10 - 15 |  |
| linear shrinkage after 168 hours @ 70 °C | max. 4% | ASTM D 1204 |
| elongation | min. 220% | ASTM D 412 |
| tensile strength | 13 kg/cm2 (1300 kPa) | ASTM D 412 |
| tear resistance | 4,2 kg/cm (0,42 kN/m) | ASTM D 624 |
| compression strength (at 25%) | 0,65 kg/cm2 (65 kPa) | ASTM 1056/85 |
| compression set 50% @ 22 hours | 15% | ASTM D 395 |
| water absorption | 2% | ASTM D 1056 |
| immersion in oil 3 (22 hours @70 °C) | 17,0% | ASTM D 471/98 |
| aging resistant (air+UV) | good |  |
| fire classification | O.K. : HF1 | UL 94 - HF1 |

Additional information:

(\*) The hardness of the cellular rubber materials is measured according to the Shore 00 standard. (\*\*) The mentioned data according to the Shore A specifications is only mentioned as a guide.


### Silicone foam TYPE 522 - white

The silicone foam rubber has a closed-cell structure and is available in sheeting, strips or cut out products.

|  |  |  |
| --- | --- | --- |
| material properties | data | standard |

|  |  |  |
| --- | --- | --- |
| cellular structure | closed |  |
| curing agent | peroxide |  |
| colour | white / crème |  |
| temperature range | -70°C / +200°C |  |
| temperature intermittent | +260°C |  |
| density (\*) | 250 Kg/m3 (+/- 40) |  |
| hardness Shore 00 (\*\*) | 55 (+/- 5) | ASTM D 2240 |
| hardness Shore A (\*\*\*) | ca. 10 |  |
| thermal conductivity | 6,4 x 10-2Wm-1K-1 | ASTM C 518 |
| compression strength (at 40%) (\*\*\*\*) | 90 kPa (+/- 40) | ASTM 1056/2000 |
| elongation | min. 150% | ASTM D 412 |
| tensile strength | min. 0,75 N/mm2 | ASTM D 412 |
| compression set 22 hours | max. 15% |  |

resistance to radiation (as expected) min. 10+5 GRAYS (10+7 RADS)

As expected

fire classification O.K. FMVSS 302 (SE) - HBF (UL94)

Additional information:

For FDA approved sheeting, please contact our technical department.

High temperature materials are available on request. (From +270°C/ peak temperature 300°) (\*) The density is measured on a 25mm diameter cord.

(\*\*) The hardness of the cellular rubber materials is measured according to the Shore 00 standard. (\*\*\*) The mentioned data according to the Shore A specifications is only mentioned as a guide. (\*\*\*\*) The compression strength is measured on material 25 mm thick.


### Polyether foam sheet SG 25 - grey

|  |  |  |
| --- | --- | --- |
| material properties | data | standard |

|  |  |  |
| --- | --- | --- |
| material | Polyurethane foam | DR 7930 / T2437 |
| cellular structure | open |  |
| colour | grey |  |
| temperature range | 25 kg/m3 |  |
| net density | 22 kg/m3 |  |
| compression stress | 3,7 kPa (0,0037 N/mm2) | ISO 3386 (40%) / DIN 53577 |
| tensile strength | 120 kPa (0,12 N/mm2) | ISO 1798 |
| elongation at break | 200% | ISO 1798 |
| compression set 75% | 4% | ISO 1856/A (22 hours at 70 °C) |
| temperature range (constant) | -10°C / +70°C |  |

Polyether foam sheet SG 25 - blue

|  |  |  |
| --- | --- | --- |
| material properties | data | standard |

|  |  |  |
| --- | --- | --- |
| material | polyurethane foam | DR 9030 / T3545 |
| cellular structure | Open |  |
| colour | Light blue |  |
| gross (spatial) density | 35 kg/m3 |  |
| net density | 33 kg/m3 |  |
| compression stress | 4,5 kPa (0,0045 N/mm2) | ISO 3386 (40%) / DIN 53577 |
| tensile strength | 110 kPa (0,11 N/mm2) | ISO 1798 |
| elongation at break | 150% | ISO 1798 |
| compression set 75% | 5% | ISO 1856/A (22 hours at 70 °C) |
| temperature range (constant) | -10°C / +70°C |  |