|  |  |  |  |  |  |  |  |  |  |  |  |  | SD 1900 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  |  | SD 1300 |  |  |
|  |  |  |  |  |  |  |  |  |  |  | SD 950 |  |  |  |
|  |  |  |  |  |  |  |  |  |  | SD 650 |  |  |  |  |
|  |  |  |  |  |  |  |  |  | SD 400 |  |  |  |  |  |
|  |  |  |  |  |  |  |  | SD 260 |  |  |  |  |  |  |
|  |  |  |  |  |  |  | SD 170 |  |  |  |  |  |  |  |
|  |  |  |  |  |  | SD 110 |  |  |  |  |  |  |  |  |
|  |  |  |  |  | SD 65 |  |  |  |  |  |  |  |  |  |
|  |  |  |  | SD 40 |  |  |  |  |  |  |  |  |  |  |
|  |  |  | SD 26 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | SD 16 |  |  |  |  |  |  |  |  |  |  |  |  |
|  | SD 10 |  |  |  |  |  |  |  |  |  |  |  |  |  |

10

specific load [N/mm²]

1

0.1

0.01

0.001

Diepolast series

# Working range

Diepolast type

# Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.010

Dynamic load: up to [N/mm²]

0.016

Load peaks: up to [N/mm²]

0.5

Values depending on form factor and apply to form factor q = 3

# Material	mixed cellular polyether-urethane

Colour	red

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m lang

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.25 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 0.048 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 0.144 N/mm² | DIN 53513 (2) |  |
| Resistance to strain | 0.011 N/mm² |  | at 10% deformation |
| Residual compression set | < 5 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 0.35 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 400 % | DIN 53455-6-4 | minimum |
| Rebound elasticity | 50 % | DIN EN ISO 8307 | ± 10% |
| Specific volume resistance | >1012 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.05 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 bis +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inflammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal flammable |

Version 1.0 from 01/04/2016

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

# Load deflection curve

SD 16

Dynamic range of use

0.020

Specific load [N/mm²]

SD 16

SD 10

0.015

Static range of use SD 10

0.010

0.005

## Recording of the 3rd loading; testing between steel plates at room temperature measured with a deflection rate of 1% of the thickness per second

Form factor q = 3

0.000

0

2	4	6

Deflection [mm]

8	10

# Modulus of elasticity

SD 10

SD 16

SD 10

SD 16

0.4

Modulus of elasticity [N/mm²]

0.3

0.2

Dynamic range of use

## Dynamic test: sinusoidal excitation with an oscillating range of ± 0.22 mm at 10 Hz and ± 0.08 mm at 30 Hz

Quasistatic modulus of elasticity: tangent modulus taken from the load deflection curve

Test according to DIN 53513 Form factor q = 3

0.1

0.0

0.000

Static range of use 0.005

0.010

0.015

0.020

Specific load [N/mm²]

# Natural frequency

SD 16

Dynamic range of use

0.020

Specific load [N/mm²]

SD 16

SD 10

0.015

Static range of use SD 10

0.010

0.005

## Natural frequency of a single-degree-of- freedom system consisting of a fixed mass and an elastic bearing consisting of Diepolast SD 10 on a stiff subgrade.

Form factor q = 3

0.000

5

Version 1.0 from 01/04/2016

10	15	20	25	30

Natural frequency [Hz]

# Correction values varying form factors

## specific load 0.01 N/mm², form factor q = 3

Static load range	Deflection

0.0105	10

8

Specific load [N/mm²]

Variation of deflection [%]

6

0.0100

4

2

0.0095

0

-2

0.0090

0.3

1	3

Form factor

-4

10	0.3

1	3	10

Form factor

## Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

10

5

0

-5

-10

-15

-20

-25

5

Variation of the natural frequency [%]

0

-5

-10

-30

0.3

1	3

Form factor

-15

10

0.3

1	3	10

Form factor

DISCLAIMER:

Version 1.0 from 01/04/2016

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certified testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

|  |  |  |  |  |  |  |  |  |  |  |  |  | SD 1900 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  |  | SD 1300 |  |  |
|  |  |  |  |  |  |  |  |  |  |  | SD 950 |  |  |  |
|  |  |  |  |  |  |  |  |  |  | SD 650 |  |  |  |  |
|  |  |  |  |  |  |  |  |  | SD 400 |  |  |  |  |  |
|  |  |  |  |  |  |  |  | SD 260 |  |  |  |  |  |  |
|  |  |  |  |  |  |  | SD 170 |  |  |  |  |  |  |  |
|  |  |  |  |  |  | SD 110 |  |  |  |  |  |  |  |  |
|  |  |  |  |  | SD 65 |  |  |  |  |  |  |  |  |  |
|  |  |  |  | SD 40 |  |  |  |  |  |  |  |  |  |  |
|  |  |  | SD 26 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | SD 16 |  |  |  |  |  |  |  |  |  |  |  |  |
|  | SD 10 |  |  |  |  |  |  |  |  |  |  |  |  |  |

10

specific load [N/mm²]

1

0.1

0.01

0.001

Diepolast series

# Working range

Diepolast type

# Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.016

Dynamic load: up to [N/mm²]

0.026

Load peaks: up to [N/mm²]

0.7

Values depending on form factor and apply to form factor q = 3

# Material	mixed cellular polyether-urethane

Colour	pink

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m lang

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.24 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 0.111 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 0.328 N/mm² | DIN 53513 (2) |  |
| Resistance to strain | 0.018 N/mm² |  | at 10% deformation |
| Residual compression set | < 5 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 0.40 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 400 % | DIN 53455-6-4 | minimum |
| Rebound elasticity | 50 % | DIN EN ISO 8307 | ± 10% |
| Specific volume resistance | >1012 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.05 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 bis +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inflammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal flammable |

Version 1.0 from 01/04/2016

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

# Load deflection curve

0.035

SD 26

0.030

Specific load [N/mm²]

SD 26

SD 16

Dynamic range of use

0.025

0.020

Static range of use SD 10 SD 16

SD 10

0.015

0.010

0.005

## Recording of the 3rd loading; testing between steel plates at room temperature measured with a deflection rate of 1% of the thickness per second

Form factor q = 3

0.000

0

2	4	6

Deflection [mm]

8	10

# Modulus of elasticity

SD 16

SD 26

SD 10

SD 16

SD 26

SD 10

0.6

Modulus of elasticity [N/mm²]

0.4

Dynamic range of use

## Dynamic test: sinusoidal excitation with an oscillating range of ± 0.22 mm at 10 Hz and ± 0.08 mm at 30 Hz

Quasistatic modulus of elasticity: tangent modulus taken from the load deflection curve

Test according to DIN 53513 Form factor q = 3

0.2

0.0

Static range of use

0.000	0.005	0.010	0.015	0.020	0.025	0.030	0.035

Specific load [N/mm²]

# Natural frequency

0.035

SD 26

0.030

Specific load [N/mm²]

SD 26

SD 16

Dynamic range of use

0.025

0.020

Static range of use SD 10 SD 16

SD 10

0.015

0.010

0.005

## Natural frequency of a single-degree-of- freedom system consisting of a fixed mass and an elastic bearing consisting of Diepolast SD 16 on a stiff subgrade.

Form factor q = 3

0.000

5

Version 1.0 from 01/04/2016

10	15	20	25	30

Natural frequency [Hz]

# Correction values varying form factors

## specific load 0.016 N/mm², form factor q = 3

Static load range	Deflection

0.0170	20

Variation of deflection [%]

0.0165	15

Specific load [N/mm²]

10

0.0160

5

0.0155

0

0.0150	-5

0.0145

0.3

1	3

Form factor

-10

10

0.3

1	3	10

Form factor

## Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

15

10

5

0

-5

-10

-15

-20

10

Variation of the natural frequency [%]

5

0

-5

-10

-25

0.3

1	3

Form factor

-15

10

0.3

1	3	10

Form factor

DISCLAIMER:

Version 1.0 from 01/04/2016

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certified testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

|  |  |  |  |  |  |  |  |  |  |  |  |  | SD 1900 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  |  | SD 1300 |  |  |
|  |  |  |  |  |  |  |  |  |  |  | SD 950 |  |  |  |
|  |  |  |  |  |  |  |  |  |  | SD 650 |  |  |  |  |
|  |  |  |  |  |  |  |  |  | SD 400 |  |  |  |  |  |
|  |  |  |  |  |  |  |  | SD 260 |  |  |  |  |  |  |
|  |  |  |  |  |  |  | SD 170 |  |  |  |  |  |  |  |
|  |  |  |  |  |  | SD 110 |  |  |  |  |  |  |  |  |
|  |  |  |  |  | SD 65 |  |  |  |  |  |  |  |  |  |
|  |  |  |  | SD 40 |  |  |  |  |  |  |  |  |  |  |
|  |  | SD 16 | SD 26 |  |  |  |  |  |  |  |  |  |  |  |
|  | SD 10 |  |  |  |  |  |  |  |  |  |  |  |  |  |

10

specific load [N/mm²]

1

0.1

0.01

0.001

Diepolast series

# Working range

Diepolast type

# Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.026

Dynamic load: up to [N/mm²]

0.040

Load peaks: up to [N/mm²]

1.0

Values depending on form factor and apply to form factor q = 3

# Material	mixed cellular polyether-urethane

Colour	orange

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m lang

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.22 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 0.129 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 0.443 N/mm² | DIN 53513 (2) |  |
| Resistance to strain | 0.026 N/mm² |  | at 10% deformation |
| Residual compression set | < 5 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 0.45 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 400 % | DIN 53455-6-4 | minimum |
| Rebound elasticity | 50 % | DIN EN ISO 8307 | ± 10% |
| Specific volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.06 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 bis +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inflammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal flammable |

Version 1.0 from 01/04/2016

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

# Load deflection curve

|  |  |  |  |  |  |  |  |  |  |  | 40 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  | SD |
| 0 |  |  |  |  |  |  |  |  |  |  |  |
| SD 4 |  |  |  |  |  |  |  |  |  |  | SD 26 |
| D 26 |  |  |  |  |  |  |  |  |  |  | D 16 |
| 6 S |  |  |  |  |  |  |  |  |  |  | S |
| SD 1 |  |  |  |  |  |  |  |  |  |  |  |

0.05

Specific load [N/mm²]

0.04

Dynamic range of use

0.03

Static range of use

0.02

0.01

## Recording of the 3rd loading; testing between steel plates at room temperature measured with a deflection rate of 1% of the thickness per second

Form factor q = 3

0.00

0

2	4	6

Deflection [mm]

8	10

# Modulus of elasticity

SD 16

SD 26

SD 40

SD 16

SD 26

SD 40

0.8

Modulus of elasticity [N/mm²]

0.6

0.4

Dynamic range of use

## Dynamic test: sinusoidal excitation with an oscillating range of ± 0.22 mm at 10 Hz and ± 0.08 mm at 30 Hz

Quasistatic modulus of elasticity: tangent modulus taken from the load deflection curve

Test according to DIN 53513 Form factor q = 3

0.2

0.0

0.00

Static range of use

0.01

0.02

0.03

0.04

0.05

Specific load [N/mm²]

# Natural frequency

S

|  |  |  |  |  |  |  |  |  |  |  | 40 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  | SD |
| 0 |  |  |  |  |  |  |  |  |  |  |  |
| SD 4 |  |  |  |  |  |  |  |  |  |  | SD 26 |
| D 26 |  |  |  |  |  |  |  |  |  |  | D 16 |
| 6 S |  |  |  |  |  |  |  |  |  |  | S |
| SD 1 |  |  |  |  |  |  |  |  |  |  |  |

0.05

Specific load [N/mm²]

0.04

Dynamic range of use

0.03

Static range of use

0.02

0.01

## Natural frequency of a single-degree-of- freedom system consisting of a fixed mass and an elastic bearing consisting of Diepolast SD 26 on a stiff subgrade.

Form factor q = 3

0.00

5

Version 1.0 from 01/04/2016

10	15	20	25	30

Natural frequency [Hz]

# Correction values varying form factors

## specific load 0.026 N/mm², form factor q = 3

Static load range	Deflection

0.028	25

20

0.026

Specific load [N/mm²]

Variation of deflection [%]

15

0.024	10

0.022	5

0

0.020

-5

0.018

0.3

1	3

Form factor

-10

10

0.3

1	3	10

Form factor

## Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

5	5

Variation of the natural frequency [%]

0

0

-5

-5

-10

-15

0.3

1	3

Form factor

-10

10

0.3

1	3	10

Form factor

DISCLAIMER:

Version 1.0 from 01/04/2016

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certified testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

SD 40

SD 26

SD 65

SD 260

SD 400

SD 650

SD 1300

SD 1900

SD 10

SD 16

SD 110

SD 170

SD 950

10

specific load [N/mm²]

1

0.1

0.01

0.001

Diepolast series

# Working range

Diepolast type

# Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.040

Dynamic load: up to [N/mm²]

0.065

Load peaks: up to [N/mm²]

2.0

Values depending on form factor and apply to form factor q = 3

# Material	mixed cellular polyether-urethane

Colour	yellow

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m lang

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.15 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 0.316 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 0.743 N/mm² | DIN 53513 (2) |  |
| Resistance to strain | 0.046 N/mm² |  | at 10% deformation |
| Residual compression set | < 5 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 0.55 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 400 % | DIN 53455-6-4 | minimum |
| Rebound elasticity | 50 % | DIN EN ISO 8307 | ± 10% |
| Specific volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.07 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 bis +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inflammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal flammable |

Version 1.0 from 01/04/2016

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

# Load deflection curve

SD 65

0.08

Specific load [N/mm²]

SD 65

SD 40

0.06

Static range of use

SD 26 SD 40

SD 26

Dynamic range of use

0.04

0.02

## Recording of the 3rd loading; testing between steel plates at room temperature measured with a deflection rate of 1% of the thickness per second

Form factor q = 3

0.00

0

2	4	6

Deflection [mm]

8	10

Dynamic range of use

SD 26

SD 40

SD 65

SD 26

SD 40

SD 65

Modulus of elasticity

1.4

1.2

Modulus of elasticity [N/mm²]

1.0

0.8

0.6

## Dynamic test: sinusoidal excitation with an oscillating range of ± 0.22 mm at 10 Hz and ± 0.08 mm at 30 Hz

Quasistatic modulus of elasticity: tangent modulus taken from the load deflection curve

Test according to DIN 53513 Form factor q = 3

0.4

0.2

0.0

0.00

Static range of use

0.02

0.04

Specific load [N/mm²]

0.06

0.08

# Natural frequency

SD 65

0.08

Specific load [N/mm²]

SD 65

SD 40

0.06

Static range of use

SD 26 SD 40

SD 26

Dynamic range of use

0.04

0.02

## Natural frequency of a single-degree-of- freedom system consisting of a fixed mass and an elastic bearing consisting of Diepolast SD 40 on a stiff subgrade.

Form factor q = 3

0.00

5

Version 1.0 from 01/04/2016

10	15	20	25	30

Natural frequency [Hz]

# Correction values varying form factors

## specific load 0.04 N/mm², form factor q = 3

Static load range	Deflection

0.042

Specific load [N/mm²]

0.041

0.040

0.039

0.038

0.037

0.3

1	3

Form factor

35

30

Variation of deflection [%]

25

20

15

10

5

0

-5

-10

10

0.3

1	3	10

Form factor

## Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

10	5

Variation of the natural frequency [%]

5

0	0

-5

-10	-5

-15

-20

0.3

1	3

Form factor

-10

10

0.3

1	3	10

Form factor

DISCLAIMER:

Version 1.0 from 01/04/2016

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certified testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

SD 26

SD 65

SD 40

SD 260

SD 400

SD 650

SD 1300

SD 1900

SD 10

SD 16

SD 110

SD 170

SD 950

10

specific load [N/mm²]

1

0.1

0.01

0.001

Diepolast series

# Working range

Diepolast type

# Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.065

Dynamic load: up to [N/mm²]

0.110

Load peaks: up to [N/mm²]

2.5

Values depending on form factor and apply to form factor q = 3

# Material	mixed cellular polyether-urethane

Colour	bright green

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m lang

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.18 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 0.453 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 1.06 N/mm² | DIN 53513 (2) |  |
| Resistance to strain | 0.073 N/mm² |  | at 10% deformation |
| Residual compression set | < 5 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 0.70 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 400 % | DIN 53455-6-4 | minimum |
| Rebound elasticity | 50 % | DIN EN ISO 8307 | ± 10% |
| Specific volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.07 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 bis +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inflammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal flammable |

Version 1.0 from 01/04/2016

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

# Load deflection curve

SD 110

0.14

0.12

Specific load [N/mm²]

SD 110

SD 65

0.10

0.08

Static range of use

SD 40 SD 65

SD 40

Dynamic range of use

0.06

0.04

0.02

## Recording of the 3rd loading; testing between steel plates at room temperature measured with a deflection rate of 1% of the thickness per second

Form factor q = 3

0.00

0

2	4	6

Deflection [mm]

8	10

Dynamic range of use

SD 40

SD 65

SD 110

SD 40

SD 65

SD 110

Modulus of elasticity

2.0

Modulus of elasticity [N/mm²]

1.6

1.2

0.8

## Dynamic test: sinusoidal excitation with an oscillating range of ± 0.22 mm at 10 Hz and ± 0.08 mm at 30 Hz

Quasistatic modulus of elasticity: tangent modulus taken from the load deflection curve

Test according to DIN 53513 Form factor q = 3

0.4

0.0

0.00

Static range of use

0.02

0.04

0.06

0.08

0.10

0.12

0.14

Specific load [N/mm²]

# Natural frequency

SD 110

0.14

0.12

Specific load [N/mm²]

SD 110

SD 65

0.10

0.08

Static range of use

SD 40 SD 65

SD 40

Dynamic range of use

0.06

0.04

0.02

## Natural frequency of a single-degree-of- freedom system consisting of a fixed mass and an elastic bearing consisting of Diepolast SD 65 on a stiff subgrade.

Form factor q = 3

0.00

5

Version 1.0 from 01/04/2016

10	15	20	25	30

Natural frequency [Hz]

# Correction values varying form factors

## specific load 0.065 N/mm², form factor q = 3

Static load range	Deflection

0.070

Specific load [N/mm²]

0.065

0.060

0.055

0.050

0.3

1	3

Form factor

40

35

Variation of deflection [%]

30

25

20

15

10

5

0

-5

-10

10

0.3

1	3	10

Form factor

## Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

10

5

0

-5

-10

-15

-20

-25

5

Variation of the natural frequency [%]

0

-5

-10

-30

0.3

1	3

Form factor

-15

10

0.3

1	3	10

Form factor

DISCLAIMER:

Version 1.0 from 01/04/2016

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certified testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

|  |  |  |  |  |  |  |  |  |  |  |  |  | SD 1900 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  |  | SD 1300 |  |  |
|  |  |  |  |  |  |  |  |  |  |  | SD 950 |  |  |  |
|  |  |  |  |  |  |  |  |  |  | SD 650 |  |  |  |  |
|  |  |  |  |  |  |  |  |  | SD 400 |  |  |  |  |  |
|  |  |  |  |  |  |  |  | SD 260 |  |  |  |  |  |  |
|  |  |  |  |  |  |  | SD 170 |  |  |  |  |  |  |  |
|  |  |  |  |  | SD 65 | SD 110 |  |  |  |  |  |  |  |  |
|  |  |  |  | SD 40 |  |  |  |  |  |  |  |  |  |  |
|  |  |  | SD 26 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | SD 16 |  |  |  |  |  |  |  |  |  |  |  |  |
|  | SD 10 |  |  |  |  |  |  |  |  |  |  |  |  |  |

10

specific load [N/mm²]

1

0.1

0.01

0.001

Diepolast series

# Working range

Diepolast type

# Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.110

Dynamic load: up to [N/mm²]

0.170

Load peaks: up to [N/mm²]

3.0

Values depending on form factor and apply to form factor q = 3

# Material	mixed cellular polyether-urethane

Colour	green

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m lang

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.12 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 0.861 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 1.86 N/mm² | DIN 53513 (2) |  |
| Resistance to strain | 0.130 N/mm² |  | at 10% deformation |
| Residual compression set | < 5 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 0.95 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 400 % | DIN 53455-6-4 | minimum |
| Rebound elasticity | 50 % | DIN EN ISO 8307 | ± 10% |
| Specific volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.08 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 bis +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inflammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal flammable |

Version 1.0 from 01/04/2016

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

# Load deflection curve

SD 170

0.24

0.20

Specific load [N/mm²]

SD 170

SD 110

0.16

Static range of use

SD 65 SD 110

SD 65

Dynamic range of use

0.12

0.08

0.04

## Recording of the 3rd loading; testing between steel plates at room temperature measured with a deflection rate of 1% of the thickness per second

Form factor q = 3

0.00

0

2	4	6

Deflection [mm]

8	10

# Modulus of elasticity

SD 65

SD 110

SD 170

SD 65

SD 110

SD 170

Dynamic range of use

3.0

Modulus of elasticity [N/mm²]

2.5

2.0

1.5

## Dynamic test: sinusoidal excitation with an oscillating range of ± 0.22 mm at 10 Hz and ± 0.08 mm at 30 Hz

Quasistatic modulus of elasticity: tangent modulus taken from the load deflection curve

Test according to DIN 53513 Form factor q = 3

1.0

0.5

0.0

Static range of use

0.00	0.04	0.08	0.12	0.16	0.20	0.24

Specific load [N/mm²]

# Natural frequency

SD 170

0.24

0.20

Specific load [N/mm²]

SD 170

SD 110

0.16

Static range of use

SD 65 SD 110

SD 65

Dynamic range of use

0.12

0.08

0.04

## Natural frequency of a single-degree-of- freedom system consisting of a fixed mass and an elastic bearing consisting of Diepolast SD 110 on a stiff subgrade.

Form factor q = 3

0.00

5

Version 1.0 from 01/04/2016

10	15	20	25	30

Natural frequency [Hz]

# Correction values varying form factors

## specific load 0.11 N/mm², form factor q = 3

Static load range	Deflection

0.120

0.115

0.110

Specific load [N/mm²]

0.105

0.100

0.095

0.090

0.085

0.080

0.075

0.3

1	3

Form factor

50

Variation of deflection [%]

40

30

20

10

0

-10

10

0.3

1	3	10

Form factor

## Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

10

5

0

-5

-10

-15

-20

-25

-30

-35

0.3

1	3

Form factor

5

Variation of the natural frequency [%]

0

-5

-10

-15

-20

10

0.3

1	3	10

Form factor

DISCLAIMER:

Version 1.0 from 01/04/2016

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certified testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

|  |  |  |  |  |  |  |  |  |  |  |  |  | SD 1900 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  |  | SD 1300 |  |  |
|  |  |  |  |  |  |  |  |  |  |  | SD 950 |  |  |  |
|  |  |  |  |  |  |  |  |  |  | SD 650 |  |  |  |  |
|  |  |  |  |  |  |  |  |  | SD 400 |  |  |  |  |  |
|  |  |  |  |  |  |  |  | SD 260 |  |  |  |  |  |  |
|  |  |  |  |  |  | SD 110 | SD 170 |  |  |  |  |  |  |  |
|  |  |  |  |  | SD 65 |  |  |  |  |  |  |  |  |  |
|  |  |  |  | SD 40 |  |  |  |  |  |  |  |  |  |  |
|  |  |  | SD 26 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | SD 16 |  |  |  |  |  |  |  |  |  |  |  |  |
|  | SD 10 |  |  |  |  |  |  |  |  |  |  |  |  |  |

10

specific load [N/mm²]

1

0.1

0.01

0.001

Diepolast series

# Working range

Diepolast type

# Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.170

Dynamic load: up to [N/mm²]

0.260

Load peaks: up to [N/mm²]

3.5

Values depending on form factor and apply to form factor q = 3

# Material	mixed cellular polyether-urethane

Colour	dark green

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m lang

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.13 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 0.931 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 2.27 N/mm² | DIN 53513 (2) |  |
| Resistance to strain | 0.170 N/mm² |  | at 10% deformation |
| Residual compression set | < 5 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 1.25 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 400 % | DIN 53455-6-4 | minimum |
| Rebound elasticity | 50 % | DIN EN ISO 8307 | ± 10% |
| Specific volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.08 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 bis +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inflammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal flammable |

Version 1.0 from 01/04/2016

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

# Load deflection curve

SD 260

0.35

0.30

Specific load [N/mm²]

SD 260

SD 170

0.25

0.20

Static range of use

SD 110 SD 170

SD 110

Dynamic range of use

0.15

0.10

0.05

## Recording of the 3rd loading; testing between steel plates at room temperature measured with a deflection rate of 1% of the thickness per second

Form factor q = 3

0.00

0

2	4	6

Deflection [mm]

8	10

# Modulus of elasticity

SD 110

SD 170

SD 260

SD 110

SD 170

SD 260

Dynamic range of use

5

Modulus of elasticity [N/mm²]

4

3

2

## Dynamic test: sinusoidal excitation with an oscillating range of ± 0.22 mm at 10 Hz and ± 0.08 mm at 30 Hz

Quasistatic modulus of elasticity: tangent modulus taken from the load deflection curve

Test according to DIN 53513 Form factor q = 3

1

0

Static range of use

0.00	0.05	0.10	0.15	0.20	0.25	0.30	0.35

Specific load [N/mm²]

# Natural frequency

SD 260

0.35

0.30

Specific load [N/mm²]

SD 260

SD 170

0.25

0.20

Static range of use

SD 110 SD 170

SD 110

Dynamic range of use

0.15

0.10

0.05

## Natural frequency of a single-degree-of- freedom system consisting of a fixed mass and an elastic bearing consisting of Diepolast SD 170 on a stiff subgrade.

Form factor q = 3

0.00

5

Version 1.0 from 01/04/2016

10	15	20	25	30

Natural frequency [Hz]

# Correction values varying form factors

## specific load 0.17 N/mm², form factor q = 3

Static load range	Deflection

0.20	60

0.18	50

Specific load [N/mm²]

Variation of deflection [%]

40

0.16

30

0.14

20

0.12

10

0.10	0

0.08

0.3

1	3

Form factor

-10

10

0.3

1	3	10

Form factor

## Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

10

5

0

-5

-10

-15

-20

-25

5

Variation of the natural frequency [%]

0

-5

-10

-30

0.3

1	3

Form factor

-15

10

0.3

1	3	10

Form factor

DISCLAIMER:

Version 1.0 from 01/04/2016

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certified testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

SD 10

SD	SD	SD

26	40	65

SD	SD	SD

260       400       650

SD	SD

1300    1900

SD 16

SD 110

SD 170

SD 950

10

specific load [N/mm²]

1

0.1

0.01

0.001

Diepolast series

# Working range

Diepolast type

# Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.260

Dynamic load: up to [N/mm²]

0.400

Load peaks: up to [N/mm²]

4.0

Values depending on form factor and apply to form factor q = 3

# Material	mixed cellular polyether-urethane

Colour	petrol

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m lang

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.11 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 1.64 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 3.63 N/mm² | DIN 53513 (2) |  |
| Resistance to strain | 0.270 N/mm² |  | at 10% deformation |
| Residual compression set | < 5 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 1.65 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 400 % | DIN 53455-6-4 | minimum |
| Rebound elasticity | 50 % | DIN EN ISO 8307 | ± 10% |
| Specific volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.08 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 bis +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inflammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal flammable |

Version 1.0 from 01/04/2016

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

# Load deflection curve

SD 400

0.5

Specific load [N/mm²]

SD 400

SD 260

0.4

0.3

Static range of use

SD 170 SD 260

SD 170

Dynamic range of use

0.2

0.1

## Recording of the 3rd loading; testing between steel plates at room temperature measured with a deflection rate of 1% of the thickness per second

Form factor q = 3

0.0

0

2	4	6

Deflection [mm]

8	10

# Modulus of elasticity

SD 170

SD 260

SD 400

SD 170

SD 260

SD 400

Dynamic range of use

8

Modulus of elasticity [N/mm²]

6

4

## Dynamic test: sinusoidal excitation with an oscillating range of ± 0.22 mm at 10 Hz and ± 0.08 mm at 30 Hz

Quasistatic modulus of elasticity: tangent modulus taken from the load deflection curve

Test according to DIN 53513 Form factor q = 3

2

0

Static range of use

0.0	0.1	0.2	0.3	0.4	0.5

Specific load [N/mm²]

# Natural frequency

SD 400

0.5

Specific load [N/mm²]

SD 400

SD 260

0.4

0.3

Static range of use

SD 170 SD 260

SD 170

Dynamic range of use

0.2

0.1

## Natural frequency of a single-degree-of- freedom system consisting of a fixed mass and an elastic bearing consisting of Diepolast SD 260 on a stiff subgrade.

Form factor q = 3

0.0

5

Version 1.0 from 01/04/2016

10	15	20	25	30

Natural frequency [Hz]

# Correction values varying form factors

## specific load 0.26 N/mm², form factor q = 3

Static load range	Deflection

0.30	60

0.28	50

Specific load [N/mm²]

Variation of deflection [%]

0.26	40

0.24	30

0.22	20

0.20	10

0.18	0

0.16	-10

0.14

0.3

1	3

Form factor

-20

10

0.3

1	3	10

Form factor

## Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

10

5

0

-5

-10

-15

-20

-25

5

Variation of the natural frequency [%]

0

-5

-10

-30

0.3

1	3

Form factor

-15

10

0.3

1	3	10

Form factor

DISCLAIMER:

Version 1.0 from 01/04/2016

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certified testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

SD 10

SD	SD	SD

26	40	65

SD	SD	SD

260       400       650

SD	SD

1300    1900

SD 16

SD 110

SD 170

SD 950

10

specific load [N/mm²]

1

0.1

0.01

0.001

Diepolast series

# Working range

Diepolast type

# Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.400

Dynamic load: up to [N/mm²]

0.650

Load peaks: up to [N/mm²]

4.5

Values depending on form factor and apply to form factor q = 3

# Material	mixed cellular polyether-urethane

Colour	blue

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m lang

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.10 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 2.72 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 5.27 N/mm² | DIN 53513 (2) |  |
| Resistance to strain | 0.370 N/mm² |  | at 10% deformation |
| Residual compression set | < 5 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 2.25 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 400 % | DIN 53455-6-4 | minimum |
| Rebound elasticity | 50 % | DIN EN ISO 8307 | ± 10% |
| Specific volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.10 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 bis +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inflammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal flammable |

Version 1.0 from 01/04/2016

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

# Load deflection curve

SD 650

0.8

Specific load [N/mm²]

SD 650

SD 400

0.6

Static range of use

SD 260 SD 400

SD 260

Dynamic range of use

0.4

0.2

## Recording of the 3rd loading; testing between steel plates at room temperature measured with a deflection rate of 1% of the thickness per second

Form factor q = 3

0.0

0

2	4	6

Deflection [mm]

8	10

# Modulus of elasticity

SD 260

SD 400

SD 650

SD 260	SD 400

SD 650

Dynamic range of use

12

Modulus of elasticity [N/mm²]

9

6

## Dynamic test: sinusoidal excitation with an oscillating range of ± 0.22 mm at 10 Hz and ± 0.08 mm at 30 Hz

Quasistatic modulus of elasticity: tangent modulus taken from the load deflection curve

Test according to DIN 53513 Form factor q = 3

3

0

Static range of use 0.0

0.2

0.4

Specific load [N/mm²]

0.6

0.8

# Natural frequency

SD 650

0.8

Specific load [N/mm²]

SD 650

SD 400

0.6

Static range of use

SD 260 SD 400

SD 260

Dynamic range of use

0.4

0.2

## Natural frequency of a single-degree-of- freedom system consisting of a fixed mass and an elastic bearing consisting of Diepolast SD 400 on a stiff subgrade.

Form factor q = 3

0.0

5

Version 1.0 from 01/04/2016

10	15	20	25	30

Natural frequency [Hz]

# Correction values varying form factors

## specific load 0.4 N/mm², form factor q = 3

Static load range	Deflection

0.48

0.44

Specific load [N/mm²]

0.40

0.36

0.32

0.28

0.24

0.3

1	3

Form factor

70

60

Variation of deflection [%]

50

40

30

20

10

0

-10

-20

10

0.3

1	3	10

Form factor

## Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

10

5

0

-5

-10

-15

-20

-25

-30

-35

0.3

1	3

Form factor

5

Variation of the natural frequency [%]

0

-5

-10

-15

-20

10

0.3

1	3	10

Form factor

DISCLAIMER:

Version 1.0 from 01/04/2016

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certified testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

SD 26

SD 40

SD 65

SD 260

SD 650

SD 400

SD 1300

SD 1900

SD 10

SD 16

SD 110

SD 170

SD 950

10

specific load [N/mm²]

1

0.1

0.01

0.001

Diepolast series

# Working range

Diepolast type

# Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.650

Dynamic load: up to [N/mm²]

0.950

Load peaks: up to [N/mm²]

5.5

Values depending on form factor and apply to form factor q = 3

# Material	mixed cellular polyether-urethane

Colour	dark blue

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m lang

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.10 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 4.57 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 10.4 N/mm² | DIN 53513 (2) |  |
| Resistance to strain | 0.590 N/mm² |  | at 10% deformation |
| Residual compression set | < 5 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 3.00 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 400 % | DIN 53455-6-4 | minimum |
| Rebound elasticity | 50 % | DIN EN ISO 8307 | ± 10% |
| Specific volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.10 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 bis +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inflammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal flammable |

Version 1.0 from 01/04/2016

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

# Load deflection curve

SD 950

1.2

1.0

Specific load [N/mm²]

SD 950

SD 650

0.8

Static range of use

SD 400 SD 650

SD 400

Dynamic range of use

0.6

0.4

0.2

## Recording of the 3rd loading; testing between steel plates at room temperature measured with a deflection rate of 1% of the thickness per second

Form factor q = 2

0.0

0

2	4	6

Deflection [mm]

8	10

# Modulus of elasticity

SD 400

SD 650

SD 950

SD 400

SD 650

SD 950

Dynamic range of use

20

Modulus of elasticity [N/mm²]

15

10

## Dynamic test: sinusoidal excitation with an oscillating range of ± 0.22 mm at 10 Hz and ± 0.08 mm at 30 Hz

Quasistatic modulus of elasticity: tangent modulus taken from the load deflection curve

Test according to DIN 53513 Form factor q = 2

5

0

Static range of use

0.0	0.2	0.4	0.6	0.8	1.0	1.2

Specific load [N/mm²]

# Natural frequency

SD 950

1.2

1.0

Specific load [N/mm²]

SD 950

SD 650

0.8

Static range of use

SD 400 SD 650

SD 400

Dynamic range of use

0.6

0.4

0.2

## Natural frequency of a single-degree-of- freedom system consisting of a fixed mass and an elastic bearing consisting of Diepolast SD 650 on a stiff subgrade.

Form factor q = 2

0.0

5

Version 1.0 from 01/04/2016

10	15	20	25	30

Natural frequency [Hz]

# Correction values varying form factors

## specific load 0.6 N/mm², form factor q = 2

Static load range	Deflection

0.75

0.70

Specific load [N/mm²]

0.65

0.60

0.55

0.50

0.45

0.40

0.35

0.3

1	2

Form factor

50

40

Variation of deflection [%]

30

20

10

0

-10

-20

-30

-40

-50

10

0.3

1	2	10

Form factor

## Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

15

10

5

0

-5

-10

-15

-20

-25

-30

-35

0.3

1	2

Form factor

10

Variation of the natural frequency [%]

5

0

-5

-10

-15

-20

10

0.3

1	2	10

Form factor

DISCLAIMER:

Version 1.0 from 01/04/2016

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certified testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

|  |  |  |  |  |  |  |  |  |  |  |  |  | SD 1900 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  |  | SD 1300 |  |  |
|  |  |  |  |  |  |  |  |  |  | SD 650 | SD 950 |  |  |  |
|  |  |  |  |  |  |  |  |  | SD 400 |  |  |  |  |  |
|  |  |  |  |  |  |  |  | SD 260 |  |  |  |  |  |  |
|  |  |  |  |  |  |  | SD 170 |  |  |  |  |  |  |  |
|  |  |  |  |  |  | SD 110 |  |  |  |  |  |  |  |  |
|  |  |  |  |  | SD 65 |  |  |  |  |  |  |  |  |  |
|  |  |  |  | SD 40 |  |  |  |  |  |  |  |  |  |  |
|  |  |  | SD 26 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | SD 16 |  |  |  |  |  |  |  |  |  |  |  |  |
|  | SD 10 |  |  |  |  |  |  |  |  |  |  |  |  |  |

10

specific load [N/mm²]

1

0.1

0.01

0.001

Diepolast series

# Working range

Diepolast type

# Recommendations for elastic bearing:

Static load: up to [N/mm²]

0.950

Dynamic load: up to [N/mm²]

1.450

Load peaks: up to [N/mm²]

6.0

Values depending on form factor and apply to form factor q = 3

# Material	mixed cellular polyether-urethane

Colour	dark violet

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m lang

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.10 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 8.16 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 21.5 N/mm² | DIN 53513 (2) |  |
| Resistance to strain | 0.930 N/mm² |  | at 10% deformation |
| Residual compression set | < 9 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 3.80 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 400 % | DIN 53455-6-4 | minimum |
| Rebound elasticity | 50 % | DIN EN ISO 8307 | ± 10% |
| Specific volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.11 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 bis +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inflammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal flammable |

Version 1.0 from 01/04/2016

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

# Load deflection curve

SD 1300

1.8

1.5

Specific load [N/mm²]

Static range of use

SD 650 SD 950 SD 1300

SD 950

1.2

SD 650

Dynamic range of use

0.9

0.6

0.3

## Recording of the 3rd loading; testing between steel plates at room temperature measured with a deflection rate of 1% of the thickness per second

Form factor q = 2

0.0

0

2	4	6

Deflection [mm]

8	10

# Modulus of elasticity

SD 650

SD 950

SD 1300

SD 650

SD 950

SD 1300

Dynamic range of use

40

Modulus of elasticity [N/mm²]

30

20

## Dynamic test: sinusoidal excitation with an oscillating range of ± 0.22 mm at 10 Hz and ± 0.08 mm at 30 Hz

Quasistatic modulus of elasticity: tangent modulus taken from the load deflection curve

Test according to DIN 53513 Form factor q = 2

10

0

Static range of use

0.0	0.3	0.6	0.9	1.2	1.5	1.8

Specific load [N/mm²]

# Natural frequency

SD 1300

1.8

1.5

Specific load [N/mm²]

Static range of use

SD 650 SD 950 SD 1300

SD 650	SD 950

Dynamic range of use

1.2

0.9

0.6

0.3

## Natural frequency of a single-degree-of- freedom system consisting of a fixed mass and an elastic bearing consisting of Diepolast SD 950 on a stiff subgrade.

Form factor q = 2

0.0

5

Version 1.0 from 01/04/2016

10	15	20	25	30

Natural frequency [Hz]

# Correction values varying form factors

## specific load 0.9 N/mm², form factor q = 2

Static load range	Deflection

1.05

1.00

0.95

Specific load [N/mm²]

0.90

0.85

0.80

0.75

0.70

0.65

0.60

0.3

1	2

Form factor

50

40

Variation of deflection [%]

30

20

10

0

-10

-20

-30

-40

-50

10

0.3

1	2	10

Form factor

## Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

20

10

0

-10

-20

-30

10

Variation of the natural frequency [%]

5

0

-5

-10

-15

-20

-40

0.3

1	2

Form factor

-25

10

0.3

1	2	10

Form factor

DISCLAIMER:

Version 1.0 from 01/04/2016

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certified testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

SD 26

SD 40

SD 65

SD 260

SD 400

SD 650

SD 1300

SD 1900

SD 10

SD 16

SD 110

SD 170

SD 950

10

specific load [N/mm²]

1

0,1

0,01

0,001

Diepolast series

# Working range

Diepolast type

# Recommendations for elastic bearing:

Static load: up to [N/mm²]

1.300

Dynamic load: up to [N/mm²]

2.000

Load peaks: up to [N/mm²]

6.5

Values depending on form factor and apply to form factor q = 3

# Material	mixed cellular polyether-urethane

Colour	violet

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m lang

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.09 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 12.0 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 35.2 N/mm² | DIN 53513 (2) |  |
| Resistance to strain | 1.340 N/mm² |  | at 10% deformation |
| Residual compression set | < 9 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 4.40 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 400 % | DIN 53455-6-4 | minimum |
| Rebound elasticity | 50 % | DIN EN ISO 8307 | ± 10% |
| Specific volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.11 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 bis +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inflammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal flammable |

Version 1.0 from 01/04/2016

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

# Load deflection curve

SD 1900

2.2

2.0

Specific load [N/mm²]

SD 1900

SD 1300

1.5

Static range of use

SD 950 SD 1300

SD 950

Dynamic range of use

1.0

0.5

## Recording of the 3rd loading; testing between steel plates at room temperature measured with a deflection rate of 1% of the thickness per second

Form factor q = 2

0.0

0

2	4	6

Deflection [mm]

8	10

# Modulus of elasticity

SD 950

SD 1300

SD 1900

SD 950	SD 1300

SD 1900

Dynamic range of use

60

Modulus of elasticity [N/mm²]

50

40

30

## Dynamic test: sinusoidal excitation with an oscillating range of ± 0.22 mm at 10 Hz and ± 0.08 mm at 30 Hz

Quasistatic modulus of elasticity: tangent modulus taken from the load deflection curve

Test according to DIN 53513 Form factor q = 2

20

10

0

Static range of use 0.0

0.5

1.0

Specific load [N/mm²]

1.5

2.0	2.2

# Natural frequency

50 mm

37.5 mm

25 mm

12.5 mm

SD 1900

2.2

2.0

Specific load [N/mm²]

SD 1900

SD 1300

1.5

Static range of use

SD 950 SD 1300

SD 950

Dynamic range of use

1.0

0.5

## Natural frequency of a single-degree-of- freedom system consisting of a fixed mass and an elastic bearing consisting of Diepolast SD 1300 on a stiff subgrade.

Form factor q = 2

0.0

5

Version 1.0 from 01/04/2016

10	15	20	25	30

Natural frequency [Hz]

# Correction values varying form factors

## specific load 1.2 N/mm², form factor q = 2

Static load range	Deflection

1.5

1.4

1.3

Specific load [N/mm²]

1.2

1.1

1.0

0.9

0.8

0.7

0.6

0.5

0.3

1	2

Form factor

60

40

Variation of deflection [%]

20

0

-20

-40

-60

-80

10

0.3

1	2	10

Form factor

## Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

40

20

0

-20

-40

-60

0.3

1	2

Form factor

20

Variation of the natural frequency [%]

15

10

5

0

-5

-10

-15

-20

-25

-30

-35

10

0.3

1	2	10

Form factor

DISCLAIMER:

Version 1.0 from 01/04/2016

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certified testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de

SD 26

SD 40

SD 65

SD 260

SD 400

SD 650

SD 1900

SD 1300

SD 10

SD 16

SD 110

SD 170

SD 950

10

specific load [N/mm²]

1

0,1

0,01

0,001

Diepolast series

# Working range

Diepolast type

# Recommendations for elastic bearing:

Static load: up to [N/mm²]

1.900

Dynamic load: up to [N/mm²]

2.800

Load peaks: up to [N/mm²]

7.0

Values depending on form factor and apply to form factor q = 3

# Material	mixed cellular polyether-urethane

Colour	bordeaux red

Delivery specifications Thickness: 12.5 mm and 25 mm

Mats:	0.5 m wide, 2.0 m long

Stripes:	max. 2.0 m lang

Other dimensions on request (also stamping and moulded parts).

| Properties | Value | Test method | Comment |
| --- | --- | --- | --- |
| Mechanical loss factor (1) | 0.09 | DIN 53513 (2) | guide value |
| Static E-modulus (1) | 20.4 N/mm² | DIN 53513 (2) |  |
| Dynamic E-modulus (1) | 78.2 N/mm² | DIN 53513 (2) |  |
| Resistance to strain | 1.840 N/mm² |  | at 10% deformation |
| Residual compression set | < 8 % | DIN EN ISO 1856 | 50%, 23°C, 70 h, 30 min after unloading |
| Tensile strength | > 5.00 N/mm2 | DIN 53455-6-4 | minimum |
| Elongation at break | > 400 % | DIN 53455-6-4 | minimum |
| Rebound elasticity | 50 % | DIN EN ISO 8307 | ± 10% |
| Specific volume resistance | >1011 Ω·cm | DIN IEC 93 | dry |
| Thermal conductivity | 0.11 W/[m·K] | DIN 52612-1 |  |
| Operating temperature | -30 bis +70 °C |  |  |
| Temperature peak | +120 °C |  |  |
| Inflammability | Class E / EN 13501-1 | EN ISO 11925-1 | normal flammable |

Version 1.0 from 01/04/2016

(1) measured at maximum limit of static application range

(2) test according to DIN 53513

All information and data is based on our current knowledge. The data are subject to typical manufacturing tolerances and are not guaranteed. We reserve the right to amend the data.

# Load deflection curve

3.5

3.0

Specific load [N/mm²]

SD 1900

2.5

2.0

Static range of use

SD 1900

Dynamic range of use

1.5

1.0

0.5

## Recording of the 3rd loading; testing between steel plates at room temperature measured with a deflection rate of 1% of the thickness per second

Form factor q = 1.25

0.0

0

2	4	6

Deflection [mm]

8	10

# Modulus of elasticity

|  |  |  |  |  |  |  |  |  |  | SD | 1900 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | SD | 1900 |  |  |  |  |  |  |  |  |  |

Dynamic range of use

120

Modulus of elasticity [N/mm²]

100

80

60

40

20

## Dynamic test: sinusoidal excitation with an oscillating range of ± 0.22 mm at 10 Hz and ± 0.08 mm at 30 Hz

Quasistatic modulus of elasticity: tangent modulus taken from the load deflection curve

Test according to DIN 53513 Form factor q = 1.25

0

Static range of use

0.0	0.5	1.0	1.5	2.0	2.5	3.0	3.5

Specific load [N/mm²]

# Natural frequency

3.5

3.0

Specific load [N/mm²]

SD 1900

2.5

2.0

Static range of use

SD 1900

Dynamic range of use

1.5

1.0

0.5

## Natural frequency of a single-degree-of- freedom system consisting of a fixed mass and an elastic bearing consisting of Diepolast SD 1900 on a stiff subgrade.

Form factor q = 1.25

0.0

5

Version 1.0 from 01/04/2016

10	15	20	25	30

Natural frequency [Hz]

# Correction values varying form factors

## specific load 1.6 N/mm², form factor q = 1.25

Static load range	Deflection

2.1

2.0

1.9

Specific load [N/mm²]

1.8

1.7

1.6

1.5

1.4

1.3

1.2

1.1

1.0

0.9

0.3

1 1.25

Form factor

40

20

Variation of deflection [%]

0

-20

-40

-60

-80

-100

10

0.3

1  1.25	10

Form factor

## Dynamic modulus of elasticity at 10 Hz	Natural frequency

Variation of the dynamic modulus of elasticity [%]

160

140

120

100

80

60

40

20

0

-20

-40

-60

0.3

1  1.25

Form factor

60

Variation of the natural frequency [%]

40

20

0

-20

-40

10

0.3

1  1.25	10

Form factor

DISCLAIMER:

Version 1.0 from 01/04/2016

The information provided is intended only as a summary and general overview on matters of interest. The information is not intended to be comprehensive nor does it constitute expert advice. P+S Polyurethan-Elastomere GmbH Co.KG shall not be liable for incidental and/or consequential damages directly or indirectly sustained, nor any loss caused by not complying with relevant industry/product standards and improper use of any Diepolast products. Due to varying construction methods, any other circumstances not stated above should be brought to the attention of P+S Polyurethan-Elastomere GmbH Co.KG for review. For suitability to the prevailing site conditions, it is advised that certified testing should be conducted. It is recommended to seek further advice on your application with our technical staff prior to use.

The data sheet is not subject to any change service! All information is without guarantee. Latest version of this document available on www.pus-polyurethan.de